## Slide 1: IH2655 Seminar January 26, 2016
Electrical Characterization,B. Gunnar Malm
gunta@kth.se

## Slide 2: Outline
Background (material from IH2652 in particular review by Deen)
Process flow & measurements (suggested reading)
In-line (on-wafer) measurements and test-structures (process-control monitors)
Measurement types examples of IV and CV and process stability

## Slide 3: Process flow & measurements
Monitor starting wafer resistivity
Monitor ion-implantations in patterned regions (wells and contacts), requires monitor wafer plus physical methods
Monitor gate dielectric stack through IV, CV and reliability measurements
Monitor back-end through specific contact resistivity and sheet resistance (interconnects). Also electromigration issues
Monitor CD-control, particle contamination
Front-end to back-end

## Slide 4: Process flow & measurements
Most of the Chapters in Plummer have a subsection called:
Mesurement Methods
  Electrical measurements
3.4.1.2 Sheet resistance on page 113
4.4.1 Particle control on pages 171-172
5.4.3 Etched features on pages 244-246
6.4.3 The MOS Capacitor on page 301
7.4.3-4 Sheet resistance & Capacitance-Voltage on page 398- (also 2D methods)
11.4.2 Contact resistance/transfer length/oxide breakdown/accel. testing p.726
Front-end to back-end

## Slide 5: Examples from Plummer

## Slide 6: Examples from Plummer

## Slide 7: Test structures
All measurements are typically on a 200-300 mm inch wafer. Map statistics at selected locations
Process control monitors located at edge of die (pads in line/row)
Special test dies
of structures for in-line probe-card measurement (PCM)

## Slide 8: Device under test (DUT)
MOS capacitances for dielectrics 4-terminal resistance structures
    Van der Pauw for sheet resistance of metals, silicides, implanted/activated dopants
    Cross Bridge Kelvin for contact resistance (metal-to-semiconductor)
Different MOSFET transistors (gate length and width)rays

## Slide 9: Interconnects needed for electrical probing!
http://www.eetimes.com/document.asp?doc_id=1324343

## Slide 10: Measurement setup
Automatic wafer prober http://www.kth.se/ict/forskning/ickretsar/kiselbaserade-kompontenter
micromanipulators with needle probes or probe cards

## Slide 11: Test-structure PADS
S
B
G
D
4-15 metal layers for interconnects. Top layer thick and soft metal (Al or Au few microns)
First metal layer for in-line testing in cleanroom=fab
area 80x80 m, pitch m 100

## Slide 12: Array of DUTs vs bonding pads

## Slide 13: In-line process control monitors
Process control monitors located at edge of die (pads in line/row)
Common layout serpentine/folded lines

## Slide 14: Characterization types
IV/DC with source/measure units (SMUs), possibly preamplifiers below 1pA
  High current (example small resistance of metal/silicide line or contact)
  Low current (gate and junction leakage, charge pumping)
  Pulsed to get information about defects and avoid self-heating
AC: Impedance and C-V mainly for MOS gate oxide but also channel mobility

## Slide 15: The 4-point principle (Kelvin)
Separate voltage and current

## Slide 16: Test-structure layout for resistance
Cross-bridge Kelvin
Contact resistance, metal to highly doped silicon or
Metal to silicide

## Slide 17: Test-structure layout for resistance
Cross-bridge Kelvin

## Slide 18: Test-structure layout for resistance
Van der Pauw: 2 current terminals + 2 voltage sense terminals, different length of resistor lines
Metal or metal silicide lines, approx 10 – 1000 

## Slide 19: Examples from Plummer

## Slide 20: MOS gate oxide process stability
IV - oxide integrity, leakage current, breakdown field, charge-to-breakdown (QDB, TDDB) , hot-carrier injection (HCI), stress (NBTI)
CV - thickness (TOX), trapped charge, interface states

## Slide 21: Interpretation of real life MOS CV data
The set of CV curves from a wafer contains information about the charge in traps and interface states. Shift with respect to ideal curve shows the type of effect present.

## Slide 22: MOS CV-curves
Sweep direction
Delta ’Vfb’ hysteresis
Shift in Vfb
The set of CV curves from a wafer contains information about the charge in traps and interface states and TOX
Shift with respect to ideal curve shows the type of effect present

## Slide 23: How to interpret CV-data

## Slide 24: Monitoring of process stability
Gate length variation - critical dimension (CD) control
Monitor gate electrode in 4-point resistor configuration across wafer, plot in Weibull graph

## Slide 25: Examples from Plummer

## Slide 26: Summary
We have followed the process flow and identified need for measurements for starting wafer, front-end and back-end
Placement of process control monitors and layout of pads introduced

## Slide 27: L4: Seminar - Concept Test 4.2
Electrical characterization is used to evaluate new materials: Which statements are true?
(One or more answers may be correct)
Capacitance-Voltage (CV) is the best technique to probe defects and thickness of thin oxides
Current-Voltage (IV) is the best technique to probe defects and thickness of thin oxides
Both IV and CV are needed to probe defects in thin oxides
Both IV and CV are needed to probe thickness of thin oxide
None of the above.

## Slide 28: Seminar: Electrical Characterization - Concept Test 3.1
3.1 Electrical characterization is an important step in the wafer fabrication flow: Which statements are true?
(One or more answers may be correct)
Measurements are usually done on completed wafers
Measurements are usually done during the process flow
Measurements are usually done on special test structures
Measurements are usually done on transistors
None of the above.