## Slide 1: Time-Resolved Luminescence
―Equipment and Kinentic description of the process
Seminar for course SK3889
Lige Liu
06-11-2017
(pp. 67-122)

## Slide 2
1. Technique of Time-Resolved luminescence
1.1 Lifetime and decay curve
1.2 Time-correlated single photon counting technique
2. Kinetic description of luminescence process
2.1 Radiative and non—radiative recombination
2.1 Monomolecular process
2.3 Bimolecular process
2.4 Multiple process
3. Phonons and their participation in optical phenomena
3.1 Lattice vibration―phonon
3.2 How charge carriers influence the lattice vibration?
3.3 How point defects influence the lattice vibration?
Contents

## Slide 3
Life-time and Decay curve
Life-time
ground state
excited state
Decay curve
Upon excitaion, the luminescence emission builds up
The time electrons stay in the excitation state—life-time
After removing the excitaion, the emission decays with time prolonging

## Slide 4
Equipment
Need ultrashort laser pulse to excitate the electrons
t
WID
PER
Turn ON
Turn OFF
Rectangular pulse
Pulse generator
The pulse excitation of the sample is repeated many times and the APD record the arrival photons.
Avalanche photon-diode (APD)
photons
voltage
photoelectric effect
Spectroscopy
Digital signal
put out
Detect the emission photons, and record the arrival time of single photons when a pulse appears at the APD output
Time-correlated single photon counting

## Slide 5
Why time-resolved luminescence?
It is a route to get knowledge of the temporal behavior of the luminescence
Kinetic process of electrons/excitons
Monomolecular process
Bimolecular process
Multiple process

## Slide 6
1. Technique of Time-Resolved luminescence
1.1 Lifetime and decay curve
1.2 Time-correlated single photon counting technique
2. Kinetic description of luminescence process
2.1 Radiative and non-radiative recombination
2.1 Monomolecular process
2.3 Bimolecular process
2.4 Multiple process
3. Phonons and their participation in optical phenomena
3.1 Lattice vibration-Phonon
3.2 How charge carriers influence the lattice vibration?
3.3 How point defects influence the lattice vibration?
Contents

## Slide 7
Probability of (non-)radiative transition and quantum efficiency
Under the rule of non-equilibrium thermodynamic, the excited electrons must transition back to the ground state.
phonon (heat)
The total probability of transition to the ground state is given by
tr — radiative recombination time (radiative lifetime)
tnr — non-radiative recombination time (non-radiative lifetime)
Define the luminescence quantum yield or quantum efficiency by the ratio of radiative recombination rate to the total recombination rate as
or

## Slide 8
Monomolecular process
A localized luminescence center
Excitons are localized at a certain impurity or defect
n―The concentration of excited centres
is the number of photons absorbed in unit volume per unit time (generation term)
Eg
1/tnr
1/tr
off
The steady state
i(t)=i(0)exp(-t/t)
Single-exponential decay
Kinetic equitation
Decay state
Turn off the excitation at t=0 (=0)
n(t)=n(0)exp(-t/t)
Boundary condition n(t=0)=n(0)
i(t)=n(t)/tr
i(t) is the number of photons emitted from unit volume per unit time

## Slide 9
h is quantum efficiency, a is absorption coefficient, Iex is excitation intensity
Steady state
Double-exponential decay
i(t)=a1exp(-t/t1)+ a2exp(-t/t2)
Two kinds of localized luminescence centres
+
Monomolecular process
The steady-state-luminescence intensity exhibits a linear dependence of the excited intensity

## Slide 10
Bimolecular process
Decay state
Approximate it as i(t) ≈ t −2
Turn off the excitation at =0 (=0)
b ― the bimolecular recombination coefficiency
n ― the concentration of electrons
p ― the concentration of holes
b=bnr+ br
Kinetic equation
For the sake of simplicity, n=p
Eg
bnr
br
Excitons are not localized at a certain impurity or defect
Notes: the amplitude of the luminescence response pulse is proportional to the square of the excitation intensity I ex

## Slide 11
Bimolecular process
Steady state
The steady-state-luminescence intensity remains a linear function of the excited intensity.

## Slide 12
disorderd system
is the dispersion factor with
dispersion diffusion of photoexcited carriers
Stretched exponential
, i(t) =constant
, i(t)=i(0)exp(-t/t), reduces to the standard exponential decay.
Limiting value
, as if we ‘stretched’ an exponentially decreasing function towards later times.
lin-lin scale
log-log scale

## Slide 13
Multiple process
k ― rate constant
a ― rate constant of photocarriers
N ― the concentration of excited centres
The photothermal carriers have the highest chance to be captured by am impurity centre, promoting this into an excited state
For the sake of simplicity,
we assume 100% quantum yield
Kinetic equation:
,
, 0
Bimolecular process + thermal relaxation
Monomolecular process
Notes: N0-N the concentration of impurity centres in the ground state with the concentration of thermal electrons nt or pt

## Slide 14
In the steady state,
,
we obtain
=0
Solving the equations, we obtained,
governed by the material parameters
Multiple process

## Slide 15
Two excitation modes,
Weak excitation,
The monomolecular intensity
The bimolecular intensity
linearly
quadratically
Compare
with
All the absorbed energy is radiated in the form of monomolecular impurity luminescence. Thus,
Physical significance: almost all the photo generated carriers are trapped in the impurity centers under the low density of excitation
Multiple process
The process is dominated by monomolecular radiation.
Notes: IB varies quadratically with the excitation intensity
IM increases linearly with the excitation

## Slide 16
Strong excitation,
The monomolecular intensity
The bimolecular intensity
This is the maximum achievable intensity of the monomolecular process, which means that all the impurity centres are excited.
linearly
It swaps roles with monomolecular luminescence
Multiple process
―The total concentration of impurity atoms
The life-time of the luminescence is dominated by bimolecular radiation process.

## Slide 17
1. Technique of Time-Resolved luminescence
1.1 Lifetime and decay curve
1.2 Time-correlated single photon counting technique
2. Kinetic description of luminescence process
2.1 Radiative and non—radiative recombination
2.1 Monomolecular process
2.3 Bimolecular process
2.4 Multiple process
3. Phonons and their participation in optical phenomena
3.1 Lattice vibration―phonon
3.2 How charge carriers influence the lattice vibration?
3.3 How point defects influence the lattice vibration?
Contents

## Slide 18
Phonon
Affects the shape of the absorption edge, the wide both of the absorption and emission spectra lines
Fine structure of the spectrum
Thermal luminescence quenching

## Slide 19
The notion of phonon―lattice vibration
Atoms in a crystal keep oscillating around their equilibrium positions
The amplitudes of these oscillations rise with temperature increasing
Model: An infinite chain of identical atoms of mass m in a one-dimensional crystal
Consider interactions of the nearest neighbors and assume a harmonic approximation (harmonic oscillator), the equation of motion reads
Force constant or “spring constant”
The instantaneous deflection of the nth atom from its equilibrium position
A solution is
―the amplitude of the vibration
= , where is the wavevector and c is the velocity of wave motion

## Slide 20
We are interested in the dispersion relation
)
It is a periodic function of k
There is a maximum oscillation frequency . A continuum has no such restriction.
Near the center of the Brillouin zone (=0), the dispersion relation become nearly linear. For , can be wrote as . Such we get , which means that the discrete chain structure vanish in comparation with the wavelength. Therefore, it is in a continuum situation.
The notion of phonon―lattice vibration
Notes: It is enough to consider the range of the first Brillouin zone

## Slide 21
View the chain as an ensemble of harmonic oscillators.
(it constitutes part of Plank's blackbody radiation law)
The entire energy is
There are quasi-particles
Assign energy to every quasi-particle. We call these quasi-particle―quanta of the vibration energy ―phonon
So the phonon distribution function will be
As the temperature drops, the phonon population decay quickly.
Quantization of the vibration energy
The mean energy of a quantized harmonic oscillator at a given temperature T is
....

## Slide 22
Two kinds of oscillating atoms with different mass of m and (m)
Unit cell
Optical branch:
higher energy
Acoustic branch:
lower energy, but wider range of change with k
at =0
at
Atoms vibrate in phase. The center of the mass move like travelling in the crystal, as for sound propagation
Atoms move in counter phase―leave the center of the mass at rest
The modification
Notes: Although the one-dimensional chain of identical atoms provide us with the basic concept of the phonon, it cannot compass the full reality of a three-dimensional crystal.

## Slide 23
Actually,
Atoms oscillate along the chain axis―longitudinal vibrations
Atoms move perpendicularly to the chain―transverse vibrations
So,
Longitudinal optical phonons (LO)
Transverse optical phonons (TO)
Longitudinal acoustic phonons (LA)
Transverse acoustic phonons (TA)
In three-dimensional case,
If a crystal has n atoms per unit cell
3 types of acoustic vibration
3n-3 types of optical vibrations
Phonon

## Slide 24
How charge carriers influence the lattice vibration?
Focus on the one dimensional chain with a harmonically oscillation
In the absent of charge, the total energy is
Insert a charge into the lattice,
Introduce a new coordinate
Physically, this means that the oscillator vibrations shift to a new position accompanied by the release of relaxation energy
kinetic energy
elastic energy

## Slide 25
There are three microscopic mechanisms mediating the carrier-phonon interactions
How charge carriers influence the lattice vibration?
Atomic oscillation
Lattice vibration
Long wavelength ()
Longitudinal acoustic vibrations
Periodic expansion and compressions of the medium on a microscopic distance
The relative change in the volume of a sample
A shift in the extreme of the electron energy band
To a first approximation,
The electron wavevector
The band
Volume deformation potential of the energy level
The deformation emchanism
The piezoelectric mechanism
The Fröhlich mechanism

## Slide 26
Calculation of the deformation potential
Absolute deformation potential― difficult either in theory or experiment
Relative deformation potential ― much easier
Sample
External hydrostatic pressure
Optical measurement
Energy difference near the onset of the absorption edge
Note:
The optical phonon may partially denoted to the deformation potential, particularly the long-wavelength one.
The exciton-phonon interaction due to the deformation potential also occurs in the crystalline solids.
How charge carriers influence the lattice vibration?

## Slide 27
How charge carriers influence the lattice vibration?
The piezoelectric mechanism
For lower lattice symmetric crystal
Mechanical deformation
Electric field
Electric voltage
Piezoelectric effect
Most importantly, in the case of longitudinal acoustic modes of lattice vibrations
(Relative shift between adjacent atomic layer)
Electric field
Electric voltage
Note:
Since the piezoelectric electron-phono interaction is under long-range Coulomb forces, the interaction is strongest for long-wavelength LA-phonons.
The exciton-phonon interaction only occurs in crystals whose crystallographic point group does not contain the centre of inversion.
Deformation varies in time

## Slide 28
How charge carriers influence the lattice vibration?
The Fröhlich mechanism
The most important exciton-phonon interaction
Only occurs in
Ionic crystals
Semiconductors with ionic contribution to the lattice energy―polar semiconductors
The opposite charge ions
Thus, the energy of long-wavelength LO-phonons is always greater than TO-phonons
Long-range macroscopic electric field (or macroscopic crystal polarization)
The opposite orientation of oscillations
Long-wavelength LO-phonons
Principle:

## Slide 29
How charge carriers influence the lattice vibration?
The polarization involves two components, and they are both jointly accociate with a static dielectric constant
The electronic polarization component: the shift of the electron cloud with respect to the nuclei
Quantify the Fröhlich mechanism
The ionic polarization component: the shift of ions from their equilibrium position
At low field frequency, the potential energy at a distance r from a point charge reads
―dielectric constant of free space
―a static dielectric constant
Electric field screening by the electronic component of the lattice constituents alone is described by a high-frequency or optical dielectric constant and leads to the potential energy
Ionic polarization itself, which is due to the relative motion of anions and cations (representing the mass of the vibrating lattice), is then characterized by the difference
A crucial factor to describe the Fröhlich mechanism

## Slide 30
In practice, one introduces the coupling constant a in the form
Polaron radius― the very size of the polarization-deformed lattice region around the charge carrier
A polarized electron or hole ― Polaron (a quasi-particle)
Therefore,
An electron–polaron corresponds to a coupling constant
A hole–polaron corresponds to a coupling constant
The effective polaron mass, , is always larger than the effective mass of a ‘bare’ quasi-particle
Note:
As for exciton-phonon coupling, it is not only related to the coupling constant, but also the exciton Bohr radius
How charge carriers influence the lattice vibration?
Quantify the fröhlich mechanism
where

## Slide 31
How point defects influence the lattice vibration?
Assume that the lattice contains a single point defect (an impurity atom of mass M,≠m ≠M)
For one-dimensional chain,
An unaffected mode of the basic lattice
the spring constant f remains unchanged in its neighbourhood
(b) A low frequancy resonance mode
f ,<f, situated within the band of allowed phonon frequencies of the unpurturbed lattice
the resonance energy can transfer from the unpurturbed area leads to an amplification of the local area
(c) A local mode in superposition with the basic lattice mode
f ,>f, located above the highest allowed frequency of perfect lattice vibration ―the amplification of such mode decreases rather quickly away from the defect
Unaffected mode
Resonance mode

## Slide 32
Quantify of the localization of the mode
Assume: there are N atoms oscillating in this mode, with the same amplitudes . The potential energy of oscillating atoms in the harmonic approximation is
the total energy of a quantum harmonic oscillator, independence of N, is
which is fully determined by the frequency and temperature
Note:
Translation symmetry of the unperturbed crystal
Only optical phonons around k=0 are active
in infrared spectra and Raman scattering
Defects breaks the symmetry and modified the selections rules for infrared and Raman spectroscopy
modes from almost the entire Brillouin zone can participate in infrared and Raman experiments
How point defects influence the lattice vibration?

## Slide 33
An impurity centre related optical excitation and subsequent radiative transition
Consider a one-dimensional chain with a single type of atom in which an impurity atom of mass (≠ ) embedded
Such a defect leads to a distortion in the equilibrium positions of the nearest neighbors
The impurity atoms, just like the host atoms, oscillate around their equilibrium positions at any temperature and (assuming harmonic oscillations) we can write for the total energy of the oscillating impurity
How point defects influence the lattice vibration?
― the effective force constant determining the oscillation frequency
() ― the instantaneous displacement from the equilibrium position
―a configurational coordinate that is a simple way to describe the relative motion of a point defect and its nearest neighbors
The impurity will oscillate around a new equilibrium position, and we can write its total energy
Here we assume that the force constant remains unchanged as the atom goes to the excited electronic state, thus =

## Slide 34
One of the valence electrons jumps to a higher energy level.
The excited electron in the position of [, + ]
The energy picture of ground and excited state
How point defects influence the lattice vibration?
The equilibrium distance grows from the value to a value (> )
The ground electron in the position of [, ]
Notes: Q g0 the equilibrium distance between the impurity and its nearest neighbours of mass m, this distance generally differs from the unperturbed ‘lattice constant’ a,

## Slide 35
A→B: Upon the absorption of a suitable photon, a vertical transition from point A and B takes place
Point B has the highest occurence probability at .
B→C: The system reaches a equilibrium postion C by handing over energy (called relaxiation energy) to the lattice in the form of heat
C→D: The system drop to point D of the ground state by radiating luminescence photon of the energy
D→A: The entire process is again completed by releasing the relaxation energy equal to the energy difference between D and A
The absorption of a suitable photon proceeds extremely faster (~ 10−15 s) than the typical frequencies of lattice vibrations (ω ~ 1012 –1013 s−1), which leads to verticality of the resulting optical transitions in the configurational coordinate diagram―Franck–Condon principle
How point defects influence the lattice vibration?
Excitation and Radiation
We can immediately see that the principle inherently explains the Stokes’ luminescence law:
Notes: In its ground electronic state, the system is located on the lower parabola around the minimum A
Point B, as the final transition state, is determined by that vibronic level of the excited electronic state that has the highest occurrence probability at Q = Q g0
However, point B represents an excited vibrational state of the upper energy curve, which is a non-equilibrium position. Hence, by rearranging the configuration of its adjacent nuclei, the system gradually reaches an equilibrium given by the minimum C of the upper phonons hω e (= hω g )
At point C, the system is still in an excited electronic state of finite lifetime (10−9 –10−8 s for the allowed dipole transitions); after this time, it drops to point D of the ground electronic state, radiating a luminescence photon of energy hν lum= E C– E D.

## Slide 36
The relaxation energy
is the dimensionalless parameter called Huang–Rhys factor. This factor hence represents the mean number of phonons emitted as the centre relaxes along the path B → C or D → A
If ≠ , define two different values of the Huang–Rhys factor: and
The larger the parameter , the larger is the shift (– ) and thus the stronger is the interaction between the excited centre and its surroundings
is the lowest excitation energy to be supplied to the centre to bring it to the excited electronic state. Optically, this will certainly be possible if the axes of both parabolas merge, i.e. ≈ and → 0, or = 0.
No-phonon line
Phonon wing
How point defects influence the lattice vibration?
supposing
The lowest excitation energy

## Slide 37
The two parabolic curves intersect at point X
Putting aside zero-point oscillations, the energy separation of point X from the minimum C of the upper parabola is equal to
This is the activation energy
With temperature increasing, the amplitude of vibration of the centre around its position increase. The chance of the system reaching to point X increase. What does it meam?
It overcomes the potential barrier of height . The probability of such a thermally activated process is governed by
where (s−1) is the so-called frequency factor
How point defects influence the lattice vibration?
heat
At a temperature close to absolute zero, the excited centre is located near point C.

## Slide 38
Thermal quenching of the luminescence
drops with increasing temperature and this effect is called thermal quenching of the luminescence
Note:
The above analysis of thermal quenching was based on the assumption that the intersection point X is at a higher energy than point B. If both points are located on the same level or if X is even lower than B then there will be a steep drop in luminescence intensity since a non-radiative transfer of the electronic excitation energy to the matrix will prevail already at very low temperatures.
How point defects influence the lattice vibration?

## Slide 39
The shape of absorption and emission spectra of a localize centre
At first glance, it may seem that both the absorption and emission are formed by narrow lines corresponding to the transitions A → B and C → D.
However, the truth is somewhat more complicated. The ‘harmonic oscillators’ of the ground as well as the excited electronic states oscillate incessantly, and so both the initial and the final point of an optical transition must respect the spatial distribution of the oscillator probability density.
So, for absorption spectrum:
It will consist of a series of narrow lines spaced equidistantly by the phonon energy , and their intensities will be modulated by a certain probability distribution.
For emission spectrum: mirror-like with respect to the absorption spectrum
At absolute zero temperature, this yields the shape of the absorption spectrum to be given by the Poisson distribution
where numbers the vibrational level of the excited electronic state.
How point defects influence the lattice vibration?

## Slide 40
At =0， single line cooresponds to the zero-phonon transition―no-phonon line
Medium
Strong
Various strength of the exciton-phonon coupling:
Weak
With increasing,
The intensity of the no-phonon line decreases;
Appear phonon replicas or satellites at higher ;
The maximum of the spectral ‘envelope’ occurs roughly at ;
The phonon satellites gradually merge into a continuum―phonon wing.
The ratio of the no-phonon line intensity to the total intensity of the absorption (or emission) band (+ ) is called the Debye–Waller factor
A distinct no-phonon line;
A negligible phonon wing;
Zero Stokes shift;
A large factor .
An inconspicuous no-phonon line;
A number of phonon satellites;
Phonon wing (up to ≈ 10);
A small factor 10−2.
The no-phonon line missing completely;
A broad phonon wing;
A large Stokes shift;
Poisson distribution → Gaussian form ( ≥ 10);
A small factor 0.
How point defects influence the lattice vibration?

## Slide 41
Thanks for your attentions!

## Slide 42
定义被激发电子停留在激发态的平均时间称为荧光寿命，荧光寿命代表分子轨道更加详细的组成及复合机理。荧光寿命通常在ps到us级。如此短的时间过程，我们无法直接采 用现有的电子及检测手段准确获取ps级间隔的数据，所以以统计学为基础的时间相关单光子计数方法（TCSPC）成为最成熟、最准确、灵敏度最高的荧光寿命测试方法。
荧光寿命的物理模型是δ脉冲光源激发，样品发射荧光，荧光强度对应这个δ脉冲的响应。实际的光源中，脉宽都是存在的，于是我们把脉宽分解为多个δ脉冲的集合，实际获取的荧光寿命成为这个集合的响应的加和。高等数学上面称之为卷积，
随后通过数学解卷积过程，我们就获得准确的样品的荧光寿命及组成。
对于TCSPC测试过程，整个荧光衰减过程采用时间通道的方案来进行，通常时间通道有256-8096个供选择，统计假设采集到光子的概率和当时的荧光强度成正比。脉冲光源开始工作时，我们获取计时Start信号，设定检测器在一次脉冲获取一个光子的概率是2%，通过TAC时幅转换器把获得光子的时间（start to stop）以电压形式记录下来，记录在对应的时间通道中；多次脉冲后，多通道时间记录器中就获得了实际的荧光衰减曲线；然后我们以同样的方法采集光源的脉宽曲线。荧光衰减曲线和光源脉宽曲线带入专门的拟合软件，我们可以获得荧光寿命的数值、组成及相关系数。
电压输出一个数字信号并在多道分析仪(Multichannel Analyzer)的相应时间通道计入一个信号,表明检测到寿命为该时间的一个光子。几十万次重复以后,不同的时间通道累积下来的光子数目不同。以光子数对时间作图可得到荧光衰减曲线。

## Slide 43
时间相关单光子计数(Time-correlated single photon counting, TCSPC)、相调制(Phase modulation method)和频闪(strobe techniques)等三种现代荧光寿命测定方法
相调制与TCSPC不同之处在于样品被正弦调制的激发光激发
频闪技术: 与脉冲光源同步,电压脉冲启动或按一定程式延迟启动光电倍增管,光电倍增管按预设时间门(Δt)检测样品的荧光强度
t
WID
PER
Turn ON
Turn OFF
Quantum dot
Localized center
electron
hole
(t p → ∞)