## Slide 1
Bound excitons and highly excited semiconductors
p. 180 – p. 239
Thomas Lettner

## Slide 2: Overview
  7.2 Bound excitons
8 Highly excited semiconductors
  8.1 Experimental considerations
  8.2 Excitonic molecule or biexciton
  8.3 Collisions of free excitons
  8.4 Electron–hole liquid (EHL)
  8.5 Electron–hole plasma (EHP)
  8.6 Bose–Einstein condensation of excitons

## Slide 3: Bound excitons
Lattice defects, especially impurity atoms
Intentional: doping
Unintentional: residual impurity
Very efficient potential wells (traps) for free excitons (FE)
Localization: FE loses its kinetic energy
Result: Bound excitons (BE)
Extrinsic luminescence with high efficiency

## Slide 4: Capture of excitons
Typical Wannier exciton radius:
Capture cross-section:
Typical impurity concentration:
Thermal velocity of excitons diffusion: ()
Mean free exciton lifetime before trapping:
Note: of FE in direct semiconductor similar. For indirect semiconductor

## Slide 5: Bound excitons in Si
Nominally pure Si
Doped with (B + As)

## Slide 6: Typical BE characteristics
Strong emission and low lifetime (Giant oscillator strength)
Narrow emission lines (Spread excited area)
No broadening with temperature (Kinetic energy = 0)
Intensity linear with excitation power (Saturation at high power)
Red-shifted with respect to FE
No phonon
Phonon assisted

## Slide 7: Types of bound excitons
Excitons bound to
shallow impurities (neutral, ionized)
Isoelectronic impurities
Bound multiexciton complexes (BMEC)
Self-trapped excitons

## Slide 8: Excitons bound to ionized impurities
  Capturing of free exciton (FE) by an ionized donor
  exciton bound to ionized donor
  dissociation or binding energy in the complex
  bound exciton photon emission energy
Analogous with ionized acceptors

## Slide 9: Stability of BE ionized impurity complexes
: the hole can escape easier
Hole heavier
Electron heavier
: the electron can escape easier
neutral remainder:
neutral remainder:
Stable for

## Slide 10: Thin layer of GaAs at 2 K

## Slide 11: Excitons bound to neutral impurities
  Capturing of free exciton (FE) by an ionized donor
  exciton bound to a neutral donor
  exciton binding energy in the complex
  bound exciton photon emission energy
Analogous with ionized acceptors
Notes: Indirect bandgap semiconductor needs a phonon hw

## Slide 12: Stability of BE neutral impurity complexes
Compare with
Compare with
or
Thin GaAs at 2K

## Slide 13: Haynes rule
depends on chemical nature (central cell correction)
Not universal
Modified for GaP
Not accepted in II-VI semiconductors
Modified for GaP

## Slide 14: Bound multiexciton complexes (BMEC)
Multiple (m) excitons localized
Neutral donor or acceptors
Less localization with increasing m
“shell model”
Note: Level splitting due to higher number of electron and hole states adds weaker emission lines

## Slide 15: Quantitative luminescence analysis in Si
1982 Tajima for weakly doped Si wafers
, TO-phonon assisted
Supplementing to other methods
PTO(BE)/ITO(FE) ~ NP
BTO(BE)/ITO(FE) ~ NB
Notes: Strong pumping (EHL)
Sample cooling (evaporation of BE)
High accuracy Fourier approach (increased S/N ratio)
Calibration curves also for Al, Ga and As
Materialrs CdTe, and GaAs tricky (residual impurities)

## Slide 16: Excitons bound to isoelectronic impurities
Substitutional atom from same group
GaP/N, AgBr/, KCL/Tl, CsI/Tl
Difference in electronegativity (X)
Example: GaP/N
Localization process:
  captures a free electron using short range forces
  attracts a free hole using long range forces
Localization of the excitation: change in Exciton-phonon coupling, Huang-Rhys factor

## Slide 17: GaP and AgBr
GaP/N:
  Small Huang-Rhys factor ,
  narrow lines
  A: exciton in J=1 state
  B: exciton in J=2 state
AgBr/:
  Large Huang-Rhys factor ,
  broad band
Effective enhancement
Notes: Absence of Auger recombination (only two quasi particles)
Strong delocalization = large uncertainty in k-space, hence transition becomes allowed
Quasi-direct radiative recombination

## Slide 18: Enhancement for isoelectric impurities
Reasons:
Efficient trapping
Absence of Auger non-radiative recombination (only two quasi particles involved)
Strong localization in real space (Δx Δk ≥ ½) quasi-direct radiative recombination
Compare exciton bound to shallow impurity:
Long-range coulomb forces
Auger recombination for neutral donor/acceptors
Always narrow lines (weak localization)
Extremely high enhancement (in indirect bandgap semiconductors)

## Slide 19: Self-trapped excitons (STE)
Requirements:
  Polar semiconductor
  Strong exciton-phonon interaction
Result: Polaron formation
Free (F) and self-trapped (S) states
Short-range forces redistribute atoms lattice relaxation energy: coupling constant:
Fröhlich mechanism (LO – phonons) long-range forces absent in IV homopolar semiconductors coupling constant: (B is the total energy width of the exciton band)

## Slide 20: Self-trapped exciton luminescence
Intrinsic luminescence process
Even in pure and unperturbed lattice
Broad emission spectrum
Free and ST excitons may coexist
Compare AgBr and AgCl:
Similar chemical properties
Complete different spectrum
Reason: in AgCl
17
Cl
35
Br
9
F
Group 7

## Slide 21: Self-trapping mechanism in AgCl
Formation of
Valence band maximum comprises of:
3p states of 4d states of
Jahn-Teller effect: lowered symmetry of the complex (prolonged axis of the complex)
Contribute to self-trapped hole wavefunction
Q = Separation of ligands
Various other microscopic mechanisms of hole self-trapping exist.

## Slide 22: Highly excited semiconductors
Excitonic molecule (biexciton)
Free electron collisions
Electron-hole liquid (EHL) and plasma (EHP)
Bose-Einstein condensation of excitons
Monomolecular generation process: (steady-state exciton concentration)
Strong interaction between excitons for
Direct bandgap requires high excitation power of 1 kW/cm² - 10 MW/cm².
Two-photon excitation for homogeneous , but even higher power ~100 MW/cm²

## Slide 23: Excitonic molecule (EM, biexciton)
Fusion of two excitons (like H2 molecule)
Binding energy for arbitrary
Typical semiconductor:
Radiative recombination:
One exciton transforms to free exciton (n=1)
Second exciton recombines, emitting a photon
Free biexcitons and biexcitons bound to impurities
Some theoretical values for calculated by different authors
typical

## Slide 24: Luminescence of free biexcitons
DIRECT
INDIRECT
Red-shift with respect to FE absorption
Maximum photon energy:
Low-energy tail (BE dispersion less curved)
Inverse Maxwell-Boltzmann distribution
Momentum conservation via recoil exciton or phonon
In general:
Note: Biexcitons are also bosons:

## Slide 25: Emission lineshape of excitonic molecules
Direct bandgap: minimum at
(JDOS)
Indirect bandgap: minimum at
High-energy edge broadens with temperature
large for and large biexciton radius (spatial extent) Can be determined through fitting

## Slide 26: Properties of excitonic molecule emission
Intensity , with
(compare mono- and bimolecular)
Binding energy
Spectral position
Thermodynamically
Exciton/Biexciton gas in potential well.
Bound biexciton:
2 excitons localized at impurity
Lineshape:
symmetric
independent to or
exhibits saturation behavior

## Slide 27: Collisions of free excitons
Inelastic collisions of two excitons X-X:
X 1 recombines ()
X 2 is excited (*) or dissociates (e-h)
New emission lines Pn:
Complicated lineshape due to numerous possible combinations of initial (K,K’) and final (k, K’’)
*
or

## Slide 28: Collision of free excitons luminescence
Properties:
High-energy threshold
Low-energy side asymmetrically broadened (due to continuum of e-h pair states)
Quadratic dependence on excitation intensity
Similar to excitonic molecule emission (M)
At high excitation collision process dominant
Both ‘M’ and ‘P’ can occur simultaneously
P-line only observed in direct-bandgap so far

## Slide 29: Electron-hole liquid (EHL)
Condensation of an exciton gas
New state of matter (Fermi liquid)
Spherical e-h drops (EHD)
Critical density of e-h pairs and critical temperature
Ground state = Σ of kinetic, exchange and correlation energies (at equilibrium )
Condensate binding energy
Very stable in polar semiconductors (LO phonons) with indirect bandgap

## Slide 30: Electron-hole liquid luminescence
Properties:
Increased probability (correlations of e-h, enhancement)
Broad band (Pauli exclusion principle)
Only for and sufficient excitation
Bandgap renormalization (low re-absorption)
Liquid density constant at fixed T
Lineshape:
Low-energy limit:
High-energy limit (T=0):
Full width (T=0):
i.e. the ground state energy of the EHL at T=0

## Slide 31: Electron-hole liquid experiments
Broad band in Ge when crossing an excitation threshold at low T.
Coexistence of EHL and M in AgBr (biexciton pocket)
Stressing of Si along [100] in order to break number of equivalent conduction band valleys and reduce
EHL emission decays faster than FE due to Auger recombination

## Slide 32: Highly excited indirect semiconductor

## Slide 33: Electron-hole plasma (EHP)
Mott insulator-metal transition
Gradual transition FE gas to e-h plasma
Metallic character (Fermi statistics)
Coulomb screening length exciton radius
Renormalization , bandgap shrinkage
and drop
Typical properties:
Low-energy emission boundary red-shifts with i.e. with excitation intensity
EHL formation can prevent
No critical temperature
Wide emission band, gets broader with

## Slide 34: Electron-hole plasma spectra - examples

## Slide 35: Bose-Einstein condensation
Macroscopic population of , fundamental consequence of quantum mechanics. Requires bosons (integer spin).
Bosonic statistics:
Total boson number finite.
Excess particles condense to the ground state (in k-space)
With critical temperature (K)
( is the free electron mass)

## Slide 36: Bose-Einstein condensation of excitons
Difficult for atomic gases (mK)
‘Easy’ for excitons: K for cm-3
Expected luminescence:
Very narrow
Low-energy edge = free exciton line
Gradual transformation (Bose narrowing)
Ideal: non-interacting excitons, lifetime, therm. dyn. equ.
Cu2O promising due to repulsive interaction and no EHP
Challenges: sample purity, high optical excitation levels
In low-dimensional systems: phase-coherent superfluid movement of a bosonic system
()

## Slide 38: Thin layer of GaAs at 2 K