## Slide 1: Radiative and non-radiative recombination in semiconductors
Hui Chen
20190924
Wallenberg Wood Science Center
Department of Fiber and Polymer Technology

## Slide 2
An excited luminescence center loses its electron excitation energy after a certain relaxation time and goes into the ground state. The transition can occur in two ways:
Radiative recombination
The excitation energy is radiated away in the form of a luminescence photon
Non-radiative recombination
The excess energy is transmitted in the form of heat (vibrations) to the crystal lattice or it can possibly cause photochemical changes in the crystal matrix or generate a lattice defect.
Introduction

## Slide 3
low-fluence or weak excitation processes
a gas-discharge lamp, an incandescent lamp or a continuous-wave gas laser with the output power of the order of 0.01–10W/cm2
high-fluence (strong) excitation processes
a pulsed laser with excitation intensity of the order of 1 kW–10MW/cm2
Classification of luminescence processes (according to the intensity of excitation)
Introduction

## Slide 4: Radiative recombination in semiconductors
Recombination of
free electron—hole pairs
a free electron with a neutral acceptor (e-A0) and of a free hole with a neutral donor (h- D0)
donor—acceptor pairs (D0—A0)
Luminescence excited by two-photon absorption
Luminescence from transition metal and rare earth ion impurities
Radiative recombination in semiconductors
The excitation energy is radiated away in the form of a luminescence photon

## Slide 5
Recombination of free electron—hole pairs
Direct bandgap case
Probability density Isp(hν) of the spontaneous emission of a photon with energy hν = E2-E1
Based on Fermi's golden rule
1. the probability of occupancy of conduction and valence band states fe(ν);
2. the quantum-mechanical probability of this transition described by the square of the matrix element of the transition |M|2;
3. the joint density of electron and hole states ρ(ν) in the corresponding bands.
Radiative recombination in semiconductors electron—hole pairs
Notes: An electron with energy E 2 situated close to the minimum of the conduction band spontaneously recom-bines with a hole situated at the top of the valence band with energy E 1 and wavector k 0 via a direct vertical transition.

## Slide 6
Factor 1: The probability of occupancy - fe(ν)
where
Fermi-Dirac distribution function
Radiative recombination in semiconductors electron—hole pairs
If: low temperature and
k B T ≪ (E g/2) ≈ E 2-E f ≈ E f-E 1
Notes: Fc: The probability of occupancy for an electron at conduction band. Fv: The probability of occupancy for a hole at valence band. At low-fluence excitation, the semiconductor can be treated as if it is still in thermal equilibrium, i.e. the Fermi level stays localized in the middle of the bandgap at low temperature . 1.380649 × 10^-23 J/K

## Slide 7
Factor 2: The quantum-mechanical probability (described by the square of the matrix element of the transition - in the dipole approximation |M|2)
M can be considered to be constant to a very good approximation over a wide range of wavevectors close to the extremes of the bands.
Radiative recombination in semiconductors electron—hole pairs
Bebb, H. B. and Williams, E. W. (1972). Photoluminescence I. Theory. In Semiconductors and Semimetals (ed. R. K.Willardson and A. C. Beer), Vol. 8, p. 181. Academic Press, New York.
Notes: the strength of the coupling between the initial and final states of the system (described by the square of the matrix element of the perturbation)

## Slide 8
Factor 3: The joint density of states ρ(ν)
The densities of states in the individual bands:
Radiative recombination in semiconductors electron—hole pairs
Kittel, C. (1976). Introduction to Solid State Physics, 5th edn. John Wiley, NewYork.
Saleh, B. E. A. and Teich, M. C. (1991). Fundamentals of Photonics. John Wiley, New York.
Notes: m e and m h stand for the effective masses of an electron and a hole, respectively

## Slide 9
Using the incremental relation
ρc(E 2)dE 2 = ρ(ν)dν
Radiative recombination in semiconductors electron—hole pairs
Notes: Mr reduced mass of the electron and hole

## Slide 10
is a parameter independent of the photon energy hν
The shape of the luminescence spectrum is also called the Maxwell-Boltzmann distribution
Radiative recombination in semiconductors electron—hole pairs
Notes: The factor ν2 comes from the photon density of states in three dimensions, which equals 4ν 2/c 3 in free space. ,Taking into account the already mentioned narrow spectral width and high optical frequencies (FWHM/hν) ≤ 0.01, how-ever, makes it possible to consider ν 2 a constant, and thus to neglect the influence of this term on the spectral lineshape.

## Slide 11: Example 1
Asymmetric curve with a tail towards the high-energy photon side
Reason: stems from the kinetic energy of recombining free electrons and holes/described by exponential distribution function
The Boltzmann tail of the Fermi-Dirac distribution broadens with increasing temperature
Radiative recombination in semiconductors electron—hole pairs
Notes: Thus, photons with higher energy are generated by these higher-energy electron-hole pairs, while the low-energy onset of the spectral line is determined by E g and its position remains fixed.

## Slide 12
Example 2
Luminescence of electron-hole pairs in Indium antimonide (InSb) at 4.2K
Soldid curve—experiment
Circles—theoretical lineshape
One possible reason for the difference at the low-energy side: influence of the slit of the monochromator, which smears the sharp onset of luminescence
Notice: for InSb, very narrow bandgap (E g ~ 0.23eV at T = 4.2K), low exciton binding energy
ensure that even at low temperatures excitons are thermally dissociated.
In nearly all other semi-conductive compounds, free electrons and holes and their luminescence are practically absent.
Radiative recombination in semiconductors electron—hole pairs
Mooradian, A. and Fan, H. Y. (1966). Phys. Rev., 148, 873.
Notes: the radiative recombination of free electrons and holes is a scarcely encountered process
low-temperature luminescence is dominated by excitonic effects,

## Slide 13: Indirect bandgap case
Direct-bandgap - same wavevector k 0
Indirect-bandgap - varying values of k
The electron excitation energy is released both in the form of luminescence and as an additional vibration energy of the lattice: E 2-E 1 = hν + hω
The probability density of spontaneous emission of a luminescence photon with energy hν = (E 2-E 1)-hω is then carried out by summing all of the contributions over the curves
Radiative recombination in semiconductors electron—hole pairs
Notes: hω denotes the energy of a phonon, which is to ensure the conservation of quasi-momentum: k hω = |k(E 2)-k(E 1)|

## Slide 14
This is obviously influenced by following factors:
1, the occupancy factors f c, f v
2, square of the absolute value of the matrix element of the optical transition |M|2
3, the densities of states ρc and ρν
Energies relative to the corresponding band edges
E e = E 2-E c for the electron and E h = E v-E 1 for the hole
reflects the summation of all contributions to the flux of emitted photons hν.
Radiative recombination in semiconductors electron—hole pairs
(Ee+Eh)
Notes: This procedure leads to the integration over all pairs of states in the conduction and valence
The upper integration limit: Ee+Eh

## Slide 15
The matrix element of the optical transition |M|2
1, vertical transitions
2, electron-phonon scattering
Ensure the indispensable alteration of quasi-momentum in the recombination event
Radiative recombination in semiconductors electron—hole pairs
The convolution-based calculation

## Slide 16
For direct bandgap
For indirect bandgap
Difference compare with the direct bandgap:
1, the red-shift of the low-energy side of the spectrum by hω
2, the replacement of the square-root dependence of the pre-exponential factor by a quadratic dependence, which slightly modifies the low-energy onset of the spectrum
the shape of the high-energy tail is most significantly influenced by the exponential factor
Radiative recombination in semiconductors electron—hole pairs
Notes: This luminescence process scarcely occurs in reality. Because of that the excited electrons and holes in an indirect-bandgap semiconductor live much longer than in direct-bandgap materials causes nearly all electrons and holes at low temperatures to be bound in excitons.

## Slide 17
Acceptor: an impurity atom in a semiconductor, whose valence is smaller by one electron than that of the main constituent of the crystal lattice, for example: boron atoms in silicon, hν ≈ E g-E A
Donor: an impurity atom in a semiconductor, whose valence is larger by one electron than that of the main constituent of the crystal lattice, for example: phosphorus atoms in silicon, hν ≈ E g-E D
Recombination of a free electron with a neutral acceptor (e-A0) and of a free hole with a neutral donor (h-D0)
Radiative recombination in semiconductors (e-A0) and (h-D0)
What is the probability of this recombination?

## Slide 18
Radiative recombination in semiconductors (e-A0) and (h-D0)
Assuming a high hole effective mass m h → ∞ and thus m h ≫ m e
Starting from recombination of free electron—hole pairs in the direct bandgap
Optical transitions across the bandgap do not carry information regarding the values of effective masses m e, m h themselves
Notes: Infinity， 无穷

## Slide 19
Radiative recombination in semiconductors (e-A0) and (h-D0)
For the recombination of the type (e-A0) the hole bound to an acceptor can be viewed as an immobile quasiparticle with an effective mass m h → ∞, (while the low-energy onset is determined by (E g-E A) instead of E g)
Similar for the neutral donor (h-D0) case

## Slide 20
Radiative recombination in semiconductors (e-A0) and (h-D0)
Example
High-purity epitaxial Gallium arsenide GaAs layer at T = 1.9K
Conditions: high purity and low temperature
1, If the semiconductor is not highly pure, another emission band (D0-A0) will clearly appear at the low-energy edge
2, Low temperatures: not only due to the effect of thermal quenching, but also to prevent the ionization of donors by the thermal energy kBT
The lattice (bath) temperature (TL)
The effective temperature of a gas of free quasiparticles (Tef）
Because: the subsystem of atoms (ions) vibrating in the lattice.
Ulbrich, R. (1973). Phys. Rev. B, 8, 5719.
Notes: However, radiative recombination (e-A0), (h-D0) is difficult to observe in an indirect-bandgap semiconductor due to the negligible concentration of free electrons and holes with respect to the concentration of excitons.
The drop of luminescence intensity with increasing temperature is called thermal quenching.
Naturally, the difference between the temperatures T ef and TL increases if a high-power excitation source is used or when the energy difference between the exciting photons and the bandgap E g rises.

## Slide 21
Radiative recombination in semiconductors (D0—A0)
Donor D0 can be considered as an ‘extra’ electron orbiting all the remaining parts of the atom, i.e. the atomic nucleus
Acceptor A0 can be treated analogously, the extra electron is substituted with a hole
Recombination of donor and acceptor (D0-A0)
Both neutral donor and acceptors are present in a semiconductor
donor +
acceptor
ionized
(D+, A−)
neutralized
(D0, A0)
Notes: free electron-hole pairs generated by the band to band excitation quickly neutralize these ionized donors and acceptors and the whole process resumes.

## Slide 22
Because of the additional energy of its (D+, A−) mutual electrostatic attraction
Radiative recombination in semiconductors (D0—A0)
Valid when the donor and the acceptor represent point charges, R ≫ r D, r A
J(R) — constitutes a non-Coulomb term, correcting for the overlap of the wavefunctions in the case of small distance R and decreasing the additional Coulomb energy. This term disappears when R is sufficiently large.
The (D0-A0) recombination manifests itself in the emission spectrum in various ways, depending on the strength of the electron-phonon coupling.
Notes: far greater than
Dielectric coefficient

## Slide 23
Radiative recombination in semiconductors (D0—A0)
Example
Luminescence spectrum: silicon- and sulphur-doped gallium phosphide, GaP, at liquid helium temperature (1.6K)
1, High photon energies (small R):
-The number of suitable neighbors (low)
-Discrete values of R are relatively scarce
sparse and weak lines
2, R increases:
-More partners
-The shells located closer to one another lines become more intense and more densely packed
3, R becomes larger
-Suitable shells nearly merge
the probability of radiative recombination W(R) decrease
Low-energy end of the spectrum gets smeared into a broad band and drops to zero somewhere above the energy limit of Eg-(EA + ED)
a = max(r D, r A)
Thomas, D. G., Gershenzon, M., and Trumbore, F. A. (1964). Phys. Rev. A, 133, 269.
Notes: silicon and sulphur are the so-called substitution donors and acceptors of type I: substitute atoms only in one of the sublattices of the crystal
Substitution donors and acceptors of type II: substitute atoms in both sublattices of the crystal, Zinc and oxygen, ZnGa-OP
The numbers next to the lines denote the number of the shell,
The lattice positions occupied by D and A in the crystal are discontinuously distributed, so the distance r between D-A can only be non-continuous values.

## Slide 24
Additional characteristic features of this type of luminescence spectrum
Radiative recombination in semiconductors (D0—A0)
blue-shift
Increasing excitation intensity
red-shift
the closest pairs with the lower R are the first ones to recombine, while pairs further and further apart start to send out luminescence in longer time delays
R
in time-resolved luminescence experiments: the increasing delay after the excitation impulse gives rise to a pronounced red-shift (low energy) of the emission spectrum
Notes: overall blue-shift of the broad band with increasing excitation intensity: gallium phosphide

## Slide 25
Radiative recombination in semiconductors (D0—A0)
Semiconductors with weak electron-phonon coupling
1, A suitable level of concentration
of both dopants
2, Low temperatures
Experimental conditions
Too low: D0 and A0 in the pairs will be too far apart from one another and no recombination will take place
Too high: the simple Coulomb interaction of D0 and A0 ceases to be valid and concentration quenching can set in.
3, The number of competing radiative recombination channels should be minimized
How narrow lines can be observed?
GaP: the only material in which a large number of narrow (D0 - A0) lines can be observed
The (D0-A0) recombination manifests itself in the emission spectrum in various ways, depending on the strength of the electron-phonon coupling.
Notes: gallium phosphide

## Slide 26
Radiative recombination in semiconductors (D0—A0)
Semiconductors with strong electron-phonon coupling
Direct-bandgap zinc sulphide ZnS with E g ~ 3.8eV
CuZn acceptors and ClS donors leads to intense green emission
1-4, increased concentration of copper
The electron-phonon coupling in this material is particularly strong, the luminescence band is broad, lacks any structure and is located far from edge emission (with large Stokes shift), near 520nm
Espe, W. (1954). Luminescent Substances in Electrical Engineering (in Czech:Luminiscenční látky v elektrotechnice. Výroba, vlastnosti a použití). SNTL, Prague.

## Slide 27
absorption of a single (suitable) photon with energy hν ex 〉 E g
generation of electron-hole pairs or excitons
radiative recombination
electron—hole pairs
(e-A0) and (h-D0)
(D0—A0)
α(hν ex) ≈ 104-105cm−1
d ≈ α−1 = 10−5-10−4 cm = 100nm-1 μm
Surface and subsurface states
The surface oxide layer
Photoluminescence
processes
Radiative recombination
influenced by
Solution: compare the emission spectra excited via one-photon and two-photon process
Radiative recombination in semiconductors
Under such conditions, the obtained spectra might not in fact reflect the properties of the studied material!!!

## Slide 28
Luminescence excited by two-photon absorption
Two-photon absorption: two photons are absorbed at the same time in a single elemental act.
energy-conservation law
Compare with the single-photon absorption (hνex>Eg)
Virtual intermediate level (Ec2):
mediates the transition between the ground (Ev) and final (Ec1) states
2hν ex = Ec1-E v.
Luminescence excited by two-photon absorption
Notes: since two-photon absorption is described in second-order perturbation theory of quantum mechanics, implying that this process is several orders of magnitude weaker than the conventional one-photon absorption (first-order perturbation theory). Thus, were the condition hνex > Eg fulfilled, intense single-photon absorption over the bandgap would set in and two-photon absorption would cease to be detectable.

## Slide 29
Luminescence excited by two-photon absorption
The hyperbolic decrease is incomparably slower
How to describe the decrease in light intensity as it passes through a semiconductor?
Thick sample is needed, for the obvious decrease of intensity
two-photon absorption coefficient
Material constant
Basov, N. G. (1966). International Conference on Physics of Semiconductors, Kyoto 1966. J. Phys. Soc. Japan, 21, Supplement, p. 277.
The decrease in the intensity of the light beam
dx: travel distance in a sample
Notes: the typical value of coeffi-cient a(~ 10−3 cm/MW) and the power density of the incident beam I 0 = 10MW/cm2, one can immediately see that—according to (5.23)—a sample length of 1cm(!) is needed so that the intensity could decrease by a single per cent (i.e. I(d)/I 0) ≈ 0.99)! Two-photon excited luminescence coming from thick samples is then, without doubt, a phenomenon connected with the bulk of the material.

## Slide 30
Bulk AgCl sample (1.5 cm) at T ≅ 80K
Ruby laser beam (hν ex = 1.78eV)
Forbidden gap width E g ≅ 3.2eV
Luminescence excited by two-photon absorption
brightness only minutely decreases
Example
Laibowitz, R. L. and Sack, H. S. (1966). phys. stat. sol., 17, 353.

## Slide 31
Luminescence spectrum of one- and two-photon excitation
Emission spectra are almost identical
Influence of surface states on luminescence is not so pronounced
Luminescence excited by two-photon absorption
Laibowitz, R. L. and Sack, H. S. (1966). phys. stat. sol., 17, 353.
Yano, S. and Ulbrich, B. (2003). Thin Solid Films, 444, 295.
Notes: Cadmium sulphide film: The spectra are shifted with respect to one another because the penetration depth of the femtosecond laser was larger than the thickness of the sample (1.58 μm); that is why the luminescence in this case is strongly influenced by reabsorption and consequently shifted to lower energies.

## Slide 32
How to recognize the observed luminescence is two and not one-photon excited?
1, ‘anti-stokes’ shift
λlum
λex
>
λex = 694 nm
λlum ≈ 500nm
Luminescence excited by two-photon absorption
hν ex ≥ hν lum
OR
Stokes’ law

## Slide 33
2, quadratic intensity dependence
Power density: I 0 = 10MW/cm2
a ≤ 10−3 cm/MW
adI 0 ≪ 1
Assume that luminescence is proportional to the absorbed power
Luminescence is proportional to the squared incident laser intensity (I0)2
Luminescence excited by two-photon absorption
From
Notes: Log-Log scale

## Slide 34
1, Impurities introduced into solids primarily in order to boost the luminescence efficiency and achieve a particular emission wavelength.
2, Cannot be easily classified from the point of view of their electrical activity as donors or acceptors, active also in the luminescence of semiconductors.
Luminescence from transition metal and rare earth ion impurities
Luminescence from transition metal and rare earth ion impurities
transition metal ions (from the fourth period of the periodic table)
rare earth ions
Impurities

## Slide 35
Luminescence from transition metal and rare earth ion impurities
Transition metal ions
exhibit luminescence as a result of transitions of electrons between the levels of the partially filled 3d shell.
3dn∗ → 3dn (∗ stands for an excited state) transitions are dipole-forbidden (Azimuthal quantum number: l = 2)
When the ions are embedded into the crystal lattice, the interaction with the electric field of the crystal makes the transitions partially allowed.
Notes: Zinc Sulphur： Manganese ion, Chromium, in aluminium oxide
Notice that 3dn∗ → 3dn (∗ stands for an excited state) transitions are, from the atomic point of view, dipole-forbidden, Because they do not comply with the condition ∆ℓ = ±1. azimuthal quantum number

## Slide 36
Luminescence from transition metal and rare earth ion impurities
rare earth ions
4fn∗ → 4fn (∗ stands for an excited state) transitions are dipole-forbidden
the crystal field makes them partially allowed
Example: luminescence of Er3+ ions built into various matrices
1, line peak approximately at 1530nm (from a, b, c)
regardless of whether they are incorporated in a matrix or in crystalline (matrix-independent)
2, the intensity of luminescence (from c, d) of Er3+ in hydrogenated amorphous silicon decreases by only about 20% when the temperature increases from 2K to 300K (temperature-independent emission)
difference with 3dn∗ → 3dn transitions: the 4f shell is strongly screened from the influence of the crystal field by the external filled orbitals (5s2 5p6)
Notes: trivalent ions of lanthanides From Cerium ions to Ytterbium ions
Example: Erbium. The emission is due to 4f11∗ → 4f11transitions from the excited state 4I 13/2 to the ground state 4I 15/2.

## Slide 37
Luminescence from transition metal and rare earth ion impurities
1, Shionoya, S. (1998). Photoluminescence. In Luminescence of Solids (ed. D. R.Vij), p. 95. Plenum Press, New York.
2, Shionoya, S. and Yen, W. M. (eds.) (1999). Phosphor Handbook, p. 141. CRC Press, Boca Raton.
3, Tanabe, Y. and Sugano, S. (1954). J. Phys. Soc. Japan, 9, 753.
Martucci, A., Guglielmi, M., Strohhöfer, C., Fick, J., Pelli, S., and Righini, G. C.(1999). Germania based sol-gel waveguides doped with Er 3+. In Innovative LightEmitting Materials. Advances in Science and Technology (ed. P. Vincenzini and G. C. Righini), Vol. 27, p. 197. Techna, Faenza.
4, Bresler, M. S., Gusev, O. B., Kudoyarova, V. Kh., Kuznetsov, A. N., Pak, P. E.,Terukov, E. I., Yassievich, I. N., Zakharchenya, B. P., Fuhs, W., and Sturm, A. (1995). Appl. Phys. Lett., 67, 3599.
5, Kaiser, W. and Garrett, C. G. B. (1961). Phys. Rev. Lett., 7, 229.
More information about luminescence from transition metal and rare earth ion impurities could be found from:

## Slide 38: Non-radiative recombination in semiconductors
Non-radiative recombination in semiconductors
----transformation of the electronic excitation energy into other types of energy than light
(i) transformation into heat
Result in local overheating and mechanical damage of the material
(ii) creation of lattice defects
Multi-phonon recombination
(iii) photochemical changes of the electronically excited material.
Auger recombination
Non-radiative
recombination
Notes: Luminescence efficiency or quantum yield almost never reaches η = 1; so where is the extra energy?

## Slide 39
Transformation of the excitation energy into heat
Transformation of the excitation energy into heat
Multi-phonon recombination
Emitted in the form of photons hν ≅ E g
Energy handed over to the lattice through n phonons with energy ℏω: Eg = nℏω
Probability for the process:
1/τ nr≈ exp(– Eg /ℏω) ≈ exp(–n)
E g≈ 2 eV and ℏω ≈ 25 meV we obtain n = 80
Wide-bandgap semiconductors outperform those with a narrow bandgap.
Very low
typical semiconductor
increases strongly in this case with the value of hν(≈ E g)
Notes: The probability of radiative transition proportion to ν 2, increases strongly in this case with the value of hν(≈ E g).

## Slide 40
Transformation of the excitation energy into heat
Non-radiative multi-phonon transitions applied in localized luminescence centre
Qe0– Qg0: the displacement from the equilibrium position
intersection point X and activation energy EA
Sequential application of one-phonon processes with participation of a real intermediate level
Strong interaction with the lattice case
Non-radiative transition in a localized luminescence center C → X → A through the emission of many local phonons
ℏω(‘cooling transitions’).
Non-radiative bimolecular recombination
mediated by ‘virtual’ electron levels
(like two-photon absorption)
Difference
Notes: Q g0 the equilibrium distance between the impurity and its nearest neighbours

## Slide 41
Transformation of the excitation energy into heat
Qe0 ≈ Qg0
Improbable
Deep level lying approximately in the middle of the bandgap (defect) mediating non-radiative recombination*
Gradual dissipation of the electron excitation energy via ‘cooling transitions’ C → C′ → C″ (defect, or deep level)
The remaining energy ‘spills’ into the matrix by a pathway of similar character C″ → C‴ → A
Shockley–Read recombination
Weak interaction with the lattice case
Probability for the process:
1/τ nr≈ exp(– E g /ℏω) ≈ exp(–n)
( Similar to bimolecular recombination)
Because
Defect associated with the deep level is always in strong interaction with the surrounding lattice
Notes: That’s why rare earth ions represent efficient luminescent centers if embedded into any lattice
The non-radiative recombination mediated by a defect is sometimes called Shockley–Read recombination.

## Slide 42
Transformation of the excitation energy into heat
Example of deep level - Surface recombination
-Takes place in a thin subsurface layer
-Conditioned by the occurrence of deep localized levels (Tamm levels)
Kinetic equations describing the generation and recombination processes
D-diffusion coefficient of the carriers
G-generation rate
n(x)-photocarrier concentration
τ-(total) non-equilibrium carrier lifetime
The surface recombination described by the recombination rate S determines the value of the derivative of n(x) at x = 0
1, The marked decrease of the concentration n(x) close beneath the surface occurs may give rise to a luminescent ‘dead layer’ with strongly reduced luminescence intensity.
2, In Figure c, the subsurface decrease of n(x) is more prominent and penetrates deeper. (Can be favorable in two-photon luminescence spectroscopy because it contributes to suppressing the spurious surface extrinsic radiative channels)
The photocarrier concentration n(x) just under the surface will decrease significantly, thus creating a concentration gradient driving photocarriers to the surface.
Notes: unoccupied bonds of surface atoms in a semiconductor give rise to these levels.
Because of the existence of the deep levels, the non-radiative recombination will be strongly inhomogeneous along the x-coordinate normal to the surface, assuming a maximum at x = 0. The photocarrier concentration n(x) just under the surface will decrease significantly, thus creating a concentration gradient driving photocarriers to the surface.
an additional term arising from the diffusion current density

## Slide 43
Transformation of the excitation energy into heat
Auger and bimolecular recombination
Based on energy and quasi-momentum conservation laws: Auger process can occur both with (a) and without (b) involvement of a quasi-momentum conserving phonon ℏΔk
no influence from a defect or impurity
Energy of the recombining pair
Passed to the third quasi-particle
For a new electronic excitation
Multi-phonon emission
Final form: heat
luminescent photon
Intrinsic Auger recombination
Notes: the no-phonon Auger process becomes feasible provided the ejected quasi-particle has to its disposal a suitable energy band, attainable without the alteration of wavevector of the (i.e.Δk= 0).

## Slide 44
Transformation of the excitation energy into heat
Kinetic equation for bimolecular recombination
Auger effect is a three-particle process, will be described by a term ~ np 2
1, The quadratic dependence on the carrier concentration signifies an important fact: the intrinsic Auger effect occurs mainly for high concentrations of free carriers. (Typical values of the Auger coefficient: A ~ 10−31 –10−29 cm6/s)
2, Intrinsic Auger recombination contributes to the fact that luminescence of narrow-bandgap semiconductors is weak.
(The easy thermal generation of free carriers across the bandgap leads to a relatively high free carrier concentration already in unexcited material)
The rate of the non-radiative process
β r (β nr): bimolecular recombination coefficient
A n, A p: Auger coefficients
Notes: d/dt denotes the derivative with respect to time,
G: the generation term,
β r (β nr) stands for the radiative (nonradiative) bimolecular recombination coefficient,
n: the concentration of electrons,
p: concentration of holes
!!!a rate of the non-radiative process (τAnr)−1
The reason is that easy thermal generation of free carriers across the bandgap leads to a relatively high free carrier concentration already in unexcited material.

## Slide 45
Transformation of the excitation energy into heat
Extrinsic Auger recombination
carriers localized at impurities
A non-radiative process accompanying luminescence originating in the transitions (e–A0 ) and (h–D0 ) and therefore decreasing its efficiency.
Condition: high concentration of free carriers or impurity atoms
(for example, to make sure the interaction of the free electron and the electron localized on a donor)

## Slide 46
Transformation of the excitation energy into heat
N: the concentration of the localized states
n = p the concentration of the excited free carriers
n N: the momentary concentration of electrons on the localized level
Conditions:
1, a relatively high concentration of the deep traps, because there has to be a positive value (N – n N)
2, a relatively high excitation to make sure n, p〉 N
Kinetic equations for electrons and holes
Notes: the process depicted in Fig has a bimolecular character, as reflected in the quadratic dependence ~ n 2
in order to ensure a sufficient concentration of electrons and holes in the extremes of the bands during rapid carrier capture in the deep trap.

## Slide 47
Creation of lattice defects
Creation of lattice defects
An electronic excitation is localized at some atom occupying a regular lattice position.
(a) Localization of the electronic excitation must occur
(b) Energy criterion.
(c) Protection against degradation to heat—phonons.
(d) Orientation criterion.
The released excitation energy is transferred to the relevant atom as a whole, which is thus ‘kicked off’ into an interstitial lattice position, creating a so-called Frenkel defect
The defect can be either transient or permanent depending on whether the interstitial atom does or does not return into its original lattice site once the excitation is terminated
Requirements:
Luščik, Č. B. and Luščik, A. Č. (1989). Decay of electronic excitations with defect formation in solids (in Russian: Raspad elektronnych vozbužděnij s obrazovaniem defektov v tverdych telach). Nauka, Moskva.
Notes: b) energy of the self-trapped exciton E e, energy E d of formation of the defect
c) self-trapped exciton gets localized must have a frequency ω ℓ higher than the highest LO-phonon frequency ωLOmax,
d) Orientation criterion. The self-trapped exciton (its charge density) should have a suitable symmetry in the crystal lattice so that the creation of the interstitial atom is energetically favourable.

## Slide 48
Photochemical changes
Photochemical changes
1, Sufficient mobility both of the electrons and of the interstitial metal ions
A photoelectron becomes captured at a certain ‘photosensitivity center’
2, Sufficiently high temperature
photochemical dissociation of the solid occurs
Silver halides AgCl, AgBr and AgI
T ≥ 200 K
A hole gets localized on a Cl− ion
Interstitial Ag+ ion
Neutral Ag0 atom
+
Trapping of other electrons
Cl2
Requirements
T ≤ 100 K
The motion of the interstitial Ag+ becomes strongly limited (‘freezes’), the formation of the latent image fades away
100–200 K
Radiative recombination, defect formation and photochemical reaction, may coexist.
The growth of a metallic silver cluster
Latent photographic image
Neutralized by the captured holes

## Slide 49
Non-radiative recombination in semiconductors
More information about non-radiative recombination in semiconductors could be found from:
1. Abakumov, V. N., Perel, V. I., and Yassievich, I. N. (1991). Nonradiative recombination in semiconductors. In Modern in Condensed Matter Sciences, Vol. 33 (ed. V. M. Agranovich and A. A. Maradudin). North Holland, Amsterdam.
2. Pilkuhn, M. H. (1981). Light emitting diodes. In Handbook on Semiconductors (ed. T. S. Moss), Vol. 4 (ed. C. Hilsum), p. 539. North Holland, Amsterdam.
3. Juška, G., Viliunas, M., Arlauskas, K., and Kočka, J. (1995-I). Phys. Rev. B, 51, 16668.
4. Luščik, Č. B. and Luščik, A. Č. (1989). Decay of electronic excitations with defect formation in solids (in Russian: Raspad elektronnych vozbužděnij s obrazovaniem defektov v tverdych telach). Nauka, Moskva.
5. Dziewior, J. and Schmid, W. (1977). Appl. Phys. Lett., 31, 346; Benz, G. and Conradt, R. (1977). Phys. Rev. B, 16, 843.

## Slide 50
Thanks for your attention!

## Slide 51
Radiative recombination in semiconductors (D0—A0)
1, The densely packed lines are hidden in the unresolved shoulder at 2.25eV
2, The wide low-energy band originally located at 2.215eV (Fig. left) is shifted to 2.20eV (in Fig. right), as a result of the thermally induced decrease in E g.
(D0-A0) radiative recombination: special example of ‘localized excitation’ without the contribution of the kinetic energy of free carriers.
‘zero-phonon’ lines
Intense zero-phonon component
Phonon sideband
luminescence spectrum of GaP at T = 20K
Notes: At this time, ∆R is 0, which means the overlap of the vibration between energy levels are maximum, non-phonon transition
To justify the application of such terminology ‘zero-phonon’ lines
weak electron-phonon coupling.
longitudinal-optical (LO) phonon energy