## Slide 1: Luminescence Spectroscopy of Semiconductors: Theory and Experiment
Electoluminescence. Quantum wells
Jianyu Wu

## Slide 2: Outline
High-field Electroluminescence
  Experimental considerations
  Mechanisms of high-field electroluminescence
  Intensity, spectral and temporal characteristics
Injection electroluminescence
  Electrical properties of a p-n junction
  Intensity, spectral and temporal characteristics of LEDs
Electroluminescence of a p-n junction biased in the reverse direction
Quantum Well
  Single quantum well with infinite barriers
  Quantum well with finite barriers
  Excitons in a quantum well
  Optical transitions in a quantum well
  Luminescence of quantum wells

## Slide 3: Outline
High-field Electroluminescence
  Experimental considerations
  Mechanisms of high-field electroluminescence
  Intensity, spectral and temporal characteristics
Injection electroluminescence
Electroluminescence of a p-n junction biased in the reverse direction
Quantum Well

## Slide 4
Fig. 11.1 Principal schematic of a sample for high-field electroluminescence studies. (b) capacitance coupling
sample subcategories:
powder phosphors thin films p-n junction
The structure of sample : non-conductive solid slab
metal electrode
active layer (~micrometres)
Transparent electrode (SnO2 , ITO, thin film metals) preparation of samples evaporation, sputtering, plasma-enhanced chemical vapour deposition (PECVD) , spin-coating
AC and DC fields DC-- fast degradation of the sample
AC--polarization effects.
No need of low temperature
of both the free electron n and hole p concentrations affect the efficiency of excitation of luminescence centres
High-field Electroluminescence
High-field Electroluminescence--Experimental considerations

## Slide 5
Fig. 11.2 Impact on the electric field distribution of semiconducting phosphor polarization by free carriers
electric-field shielding
free carrier displacement and the
formation of the space charge near electrodes
ideal rectangular voltage pulse→ considerably different shape τM the dielectric relaxation time
the mean time necessary for an extra volume charge in an insulator or semiconductor to disperse
τM = ε∞ε0/σDC
ε∞ Dielectric constant， σDC electric conductivity
ps → strongly conductive materials
us to ms → less conductive samples (typical)
High-field Electroluminescence--Experimental considerations

## Slide 6
Fig. 11.3
Possible electroluminescence processes in high fields. extrinsic luminescence centre , donor–acceptor pair , Intrinsic electroluminescence process
three potential radiative recombination channels
1. Extrinsic luminescence of localized centres (ions )
2. Recombination processes involving the participation of neutral donors and acceptors (donor–acceptor pairs )
3. Intrinsic recombination of free electron–hole pairs (very low at room temperature)
Processes of excitation of luminescence centres
electric field accelerates the free carriers
↓
inelastic collisions transfer their energy to the luminescence centres
↓
photons are emitted owing to the electron transitions between levels
(3d shell for Mn2+ ions ）
Impact ionization and excitation
High-field Electroluminescence--Mechanisms

## Slide 7
Fig. 11.4 Path evolution of an electron that is ‘heated up’ in a semiconductor in an electric field
Fig. 11.5 dependence of the electron drift velocity on the electric field intensity
electrons travel for the mean free path
Vd drift velocity of electrons
VT is the mean velocity τm is the mean time between collisions
(a) Vd << VT collision mechanism in that case remains the scattering on acoustic phonons
(b) electron system heats up, Vd Increase
mobility of electrons decrease μn, μn = μn(F).
(c) generation of optical phonons becomes the prevailing mechanism of electron scattering
High-field Electroluminescence--Mechanisms
Impact ionization and excitation

## Slide 8
Fig. 11.7 Energy band scheme of a metal–semiconductor junction (Schottky barrier)
Generation of free carriers
mechanisms of free carrier generation
1. injection of majority carriers from electrodes;
2. release of carriers from deep traps localized in the phosphor
3. release of carriers from traps on the boundary between a dielectric and the phosphor
metal and an n-type semiconductor Schottky structure
forward bias
concentration of minority remains stable
reverse bias
keeps the injected electron current
      lowered potential barrier
      tunnelling effect
accelerated electrons
High-field Electroluminescence--Mechanisms

## Slide 9
Fig. 11.8 Energy band scheme of an electron in a deep trap
Fig. 11.9 Band scheme of the interface between a dielectric and a luminescent layer
Lattice defects in semiconductors act as deep traps (potential wells) for charge carriers
application of an electric field decrease the potential barrier of the trap
thermal release of trapped electrons into the conduction band, (Poole–Frenkel effect) tunnelling through the narrowed barrier (Fowler–Nordheim tunnelling)
lattice defects are formed at the interface. electronic states are localized within the forbidden band
Generation of free carriers
High-field Electroluminescence--Mechanisms

## Slide 10
Fig. 11.11 experimental curves of the electroluminescence brightness B against the applied voltage U
Fig. 11.10 Dependence of the high-field electroluminescence brightness B on the applied voltage U
the differences between the overall curve shapes are not too important
plot in a logarithmic scale B/U 2 ∼ j/U 2 as a function of 1/U
electroluminescence intensity
High-field Electroluminescence-- characteristics
specific case of Fowler–Nordheim tunnelling:

## Slide 11
Fig. 11.12 Comparison of photoluminescence emission spectrum of mixed ZnS/CdS crystals (1, 2) with their electroluminescence spectrum (3). 1940 (b)EL (points) and PL spectra of an electroluminescence diode, 1995.
we cannot expect complete identity of both spectra because
photoluminescence emission spectrum depend on the excitation wavelength,
Electroluminescence spectrum can depend on the applied voltage, frequency of the AC field
spectral composition of electroluminescence
High-field Electroluminescence-- characteristics

## Slide 12
Fig. 11.13 Time behaviour of electroluminescence of thin films (a) SrS:Ce,K, (b) CaS:Eu and (c) ZnS:Ce,F.
temporal characteristics of electroluminescence
short flashes both during switching on and off the voltage
Infer the excitation mechanism:
pulsed voltage is switched on,
impact excitation of the Ce3+ and Eu2+
creating Ce4+ and Eu3+ ions in high electric field
Electrons released into the conduction band get subsequently localized in traps
pulsed voltage is switched off,
electrons are again released into the conduction band
captured back by ionized centres
photon is emitted due to the radiative transition inside the luminescence centre
High-field Electroluminescence-- characteristics

## Slide 13: Outline
High-field Electroluminescence
Injection electroluminescence
  Electrical properties of a p-n junction
  Intensity, spectral and temporal characteristics of LEDs
Electroluminescence of a p-n junction biased in the reverse direction
Quantum Well

## Slide 14
Fig. 11.15 Energy band scheme of a p-n junction
applying a suitable external voltage U
Excess electrons are injected from the n region to the p region
Injection electroluminescence-- Electrical properties of a p-n junction
injection electroluminescence:
the radiative recombination induced by the injection of minority carriers into a semiconductor p-n junction.
WD will decrease with increasing U

## Slide 15
Fig. 11.16
Current–voltage characteristic of a p-n junction
Fig. 11.17
Double heterostructure of P-p-N type.
rectifying properties
Injection electroluminescence-- Electrical properties of a p-n junction
js is saturation current
threshold bias Uth(≈ UD).
forward bias
reverse bias
heterojunction: an active (luminescent) region with narrower bandgap (e.g. GaAs) and a barrier region with wider bandgap
significantly improve the luminescence performance of p-n junctions:
injected electrons and holes in a narrow active region
waveguiding effect in the active region (higher refractive index)

## Slide 16
Fig. 11.18 Output light power of LED diodes as a function of the forward current.
Intensity characteristics
The onset of photon emission threshold bias ∼ Eg/e
linear increase saturation often occurs at higher current values.
blue emission is due to the recombination of donor–acceptor pairs violet emission originates from band-to-band intrinsic bimolecular recombination
carrier overflow: leakage of injected carriers from the fully occupied potential well represented by the active layer
Injection electroluminescence-- characteristics of LEDs

## Slide 17
Fig. 11.20Total (external) efficiency of injection electroluminescence in GaAs1-x Px
A sharp decrease of the efficiency
due to direct → indirect bandgap Transformation
Doping with nitrogen compensates to a large degree for this inconvenient effect
Fig. 11.19 Normalized emission spectra of LEDs by different manufacturers
Spectral characteristics
luminescence converters phosphors covering the active p-n junction of a blue LED diode in the form of a thin layer, White emission can be obtained
Minimum wavelength λm is determined by the bandgap
emission band is shifted towards longer wavelengths
extrinsic luminescence due to donor–acceptor pairs
light absorption and scattering at impurities
random fluctuations in the chemical composition of the active layer
not a smooth curves
the X–TO type and the neighbouring peak to the X–LO process.
Injection electroluminescence-- characteristics of LEDs

## Slide 18
Fig. 11.22 Example of temporal behaviour of the characteristic quantities of an LED diode:
Fig. 11.23 Definition of the rise time τr and decay time τd; An example of the frequency response of an LED diode
Temporal characteristics
the time of recombinations:
minority carrier injection, filling traps and carrier capture
electrical parameters
p-n junction represents a capacitance load for the external source
geometry of the p-n junction
rise time τr and the decay time τd as time intervals between the points corresponding to the 90% and 10% levels of signal
cut-off frequencies of LED diodes range from 10 MHz to 1 GHz
Injection electroluminescence-- characteristics of LEDs

## Slide 19: Outline
High-field Electroluminescence
Injection electroluminescence
Electroluminescence of a p-n junction biased in the reverse direction
Quantum Well

## Slide 20
Fig. 11.25
Light emission in a reverse biased p-n junction
Fig. 11.24 Electroluminescence spectrum of a silicon p-n junction
Emission spectrum is quite broad and located photon energies substantially exceeding the bandgap width.
The random and highly nonlinear character of avalanche ionization is reflected in a log-log scale
Electrical (pre-)breakdown of a reverse-biased p-n junction via the band-to-band recombination of hot e–h pairs
Electroluminescence of a p-n junction biased in the reverse direction

## Slide 21
Fig. 11.26 Electroluminescence spectrum of a commercial GaAs LED diode biased in the reverse direction.
In p-n junctions made of GaAs
component due to both direct and indirect interband transitions of hot electrons and holes
Electroluminescence of a p-n junction biased in the reverse direction

## Slide 22: Outline
High-field Electroluminescence
Injection electroluminescence
Electroluminescence of a p-n junction biased in the reverse direction
Quantum Well
  Single quantum well with infinite barriers
  Quantum well with finite barriers
  Excitons in a quantum well
  Optical transitions in a quantum well
  Luminescence of quantum wells

## Slide 23
Fig. 12.9 (a) wavefunctions, (b) dispersion relation, and (c) density of states of the four lowest quantum states.
potential energy of a quasi-particle V (z) within the well
wavefunctions and the corresponding energies:
Quantum Well--Single quantum well with infinite barriers

## Slide 24
Fig. 12.12 Wavefunctions of the first four states localized in a finite-barrier quantum well.
Fig. 12.10 The shape of the potential of a quantum well with finite barriers
In a real quantum well, the barriers are of finite height only
the number of solutions (possible localized states) depends on the barrier height V0
the deeper the well, the larger the number of localized states that can be reached
Quantum Well--Quantum well with finite barriers
Fig. 12.11 Graphical solution by the points of intersection
introduce a dimensionless variable θ and a dimensionless parameter θ0 :

## Slide 25
Fig. 12.13 Theoretical values of the exciton binding energy in a GaAs quantum layer
2D structures compared to 3D crystals :
exciton radius is decreased and the electron–hole binding interaction is increased an electron and hole are ‘squeezed’ closer together in a
relatively narrow well
in the case of real wells, one can find an optimum thickness value at which the exciton stability is maximized.
Bohr radius
Quantum Well--Excitons in a quantum well
we should consider two-particle Hamiltonian:
Containing the kinetic energies of the electron and hole, the quantum well confinement potential and the potential of the Coulomb interaction
energy levels of excitons in a two-dimensional quantum well:

## Slide 26
Fig. 12.14
absorption band undergoes a blue-shift with decreasing well width;
strengthening of excitonic effects ;
a step-like increase in the absorption background obviously take place in the well
In bulk:
the two uppermost valence bands A and B are degenerate at the point.
in quantum wells:
the confinement potential lifts this degeneracy as a result of symmetry breaking
j = 0 selection rule:
the transitions are allowed only between quantized electron and hole sub-bands with the same quantum number j.
The splitting of transitions is due to complex intermixing and splitting of the degenerate states of the uppermost valence band
Quantum Well--Optical transitions in a quantum well

## Slide 27
Fig. 12.15 Comparison of absorption (solid lines) and luminescence (dashed lines) spectra of GaAs/AlGaAs multiple quantum wells.
Luminescence spectra typically differ from absorption spectra
Only a single emission band. from the efficient relaxation of higher excited states into the lowest state,
The luminescence peak is generally shifted to lower energies: width of a real quantum well is not perfectly constant, local energy levels vary accordingly, resulting in the ‘smearing’ of energy levels
Broader spectral bands due to well thickness fluctuations *width of luminescence bands can thus be used to characterize the quality and homogeneity of the fabricated structure.
Quantum Well--Luminescence of quantum wells

## Slide 28
Fig. 12.16 Narrowing the ‘free’ exciton luminescence line when going from a 3D to a 2D structure, as a consequence of the modified shape of the density of states ρ(E) = ρ(hν).
Differences in luminescence properties of a ‘free’ exciton in a bulk semiconductor and in a 2D quantum well
1. The wavelength of excitonic luminescence from a 2D well, depends on the size of the structure (well thickness).
*quick method to extract the value of the well thickness
2. The ‘free-exciton’ emission linewidth should be more than twice as narrow in a 2D structure
*results from the differing shape of the density of states
*lowering the threshold current density for lasing
3. Excitonic phenomena are more pronounced, may be observable at room temperatures (compared to 3D crystals)
4. Nonlinear optical phenomena is much stronger and take place for much lower excitation power densities. (because of the confinement of the excited electron–hole pairs)
Quantum Well--Luminescence of quantum wells

## Slide 29
Fluctuations in the well width, chemical composition, impurity atoms, act as possible localization traps for excitons.
Excitonic emission band should be considered as inhomogeneously broadened due to the superposition of the radiative recombination of ‘free’ excitons and excitons localized in the tail states
Micro-photoluminescence technique
Fig. 12.17 Photoluminescence spectra of GaAs/AlGaAs quantum wires
Quantum Well--Luminescence of quantum wells

## Slide 30: Luminescence Spectroscopy of Semiconductors: Theory and Experiment
Electoluminescence. Quantum wells
Jianyu Wu