## Slide 1: Fråga 71
Hål är minoritetsbärare i ett n-typ kisel lager.
Hålen injeceras från en sida och diffunderar in i n-typ lagret och en koncentrationsprofil upprättshåls (steady-state) Inget ljus faller på kiselbiten och hålens driftström är försumbar. Skriv ner en diffrentialekvation som om den löses ger överskottskoncentrationen av hålen som funktion av x.

## Slide 2: Fråga 72
En p+n övergång i kisel framspänns. Vilken strömkomponent är lättast att beräkna och bestämmer strömmen?
Diffusionströmmen av hål på n-sidan
Driftström av elektroner på n-sidan
Driftström av hål på n-sidan
Diffusionströmmen av elektroner på p-sidan

## Slide 3: Figure 4.20 (a) Total J can be determined by summing JnP and JpN at the junction where both are known; (b) the other majority current components can now be determined.

## Slide 5: Figure 4.14 A forward bias reduces the junctionbarrier to ϕbi–V and allows electrons and holes to be injected over the reduced barrier.

## Slide 6: Figure 4.15 n at xp (electron density at the edge of the neutral P region) is determined by Ec – EFn. Similarly, p at xN is determined by Ev – EFp.

## Slide 7: Figure 4.18 Normalized n' and p'. n'(0) = 2p'(0) because Nd = 2Na. Ln = 2Lp is assumed.

## Slide 8
2
/
1
|)
|
(
2
)
0
(
ú
û
ù
ê
ë
é
+
=
=
r
bi
s
p
V
qN
f
e
E
E
bi
crit
s
B
qN
V
f
e
-
=
2
2
E
N
+
P
N
a
Neutral Region
0
x
p
(a)
increasing
reverse bias
x
E
x
p
(b)
increasing reverse bias
E
p

## Slide 9
V/cm
10
6
»
=
crit
p
E
E

## Slide 10
qN
V
crit
s
B
2
2
E
e
=

## Slide 12
Figure 4.34 Energy band diagram of a metal–semiconductor contact. The Schottky barrier heights depend on the metal and semiconductor materials. (a) ϕBn is the barrier against electron flow between the metal and the N-type semiconductor; (b) ϕBp is the barrier against hole flow between the metal and the P-type semiconductor.

## Slide 13
Table 4.4 Measured Schottky barrier heights for electrons on N-type silicon (ϕBp) and for holes on P-type silicon (ϕBp). (From [7].)

## Slide 14
Figure 4.35 (a) An “ideal” metal–semiconductor contact and (b) in a real metal–semiconductor contact, there is a dipole at the interface.

## Slide 15
Table 4.5 Measured Schottky barrier heights of metal silicide on Si.

## Slide 16
Figure 4.36 The potential across the depletion layer at the Schottky junction. (a) No voltage applied; (b) a negative voltage (reverse bias) is applied to the metal.

## Slide 17: Figure 4.37 ϕbi (and hence ϕB) can be extracted from the C–V data as shown.

## Slide 18: Figure 4.38 Energy band diagram of a Schottky contact with a forward bias V applied between the metal and the semiconductor.

## Slide 19: Figure 4.39 Explanation of the rectifying IV characteristics of Schottky diodes. The arrows in the subscripts indicate the direction of electron flows.

## Slide 20: Figure 4.40 Schematic IV characteristics of PN and Schottky diodes having the same area.

## Slide 21: Figure 4.41 Block diagram of a switching power supply for electronic equipment such as PCs.

## Slide 22: Figure 4.42 Illustration of quantum mechanical tunneling.

## Slide 23: Figure 4.43 A contact structure. A film of metal silicide is formed before the dielectriclayer deposition and contact-hole etching. (From [11]. © 1999 IEEE.)

## Slide 24: Figure 4.44 (a) Energy band diagram of metal–N+ Si contact with no voltage applied and (b) the same contact with a voltage, V, applied to the contact.

## Slide 25: Figure 4.45 The IV characteristics of a 0.3 µm (diameter) TiSi2 contact on N+-Si and P+-Si. (From [11]. ©1999 IEEE.)

## Slide 26: Figure 4.46 Theoretical specific contact resistance. (After [12].)