## Slide 1: Luminescence of excitons
By: Yashar Hormozan
Chapters 7 of ”Luminescence Spectroscopy of Semiconductors”
by Ivan Plant & Jan Valenta

## Slide 2: Basic types of excitons
Frenkel exciton or a small-radius exciton
  Highly localized at an atom or molecule
  Move only by a hopping mechanism
  Molecular crystals
Charge Transfer exciton
  In Ionic crystals
  Due to transfer of an electron from a lattice anion to the closest cation, creating a maximum of electron charge density
Wannier Exciton or large-radius exciton
  Electron and holes separated over many lattice constants
  Strongly delocalized wave function and free to move
  Transfer energy but not charge!

## Slide 3: Wannier exciton
Held together by Coulomb force
Similar to Hydrogen atom but larger() & unstable above T 110 K
      Due to:
    High dielectric constant in semiconductors
    Low reduced mass
Binding energy () must be higher than

## Slide 4: Absorption spectrum of Wannier exciton (Direct BG)
Zero kinetic energy
  since
The intensity drops with the state number (n)
Enhanced absorption for

## Slide 5: Absorption spectrum of Wannier exciton (Indirect BG)
The group velocity of the electron and the hole must be similar in order to create a stable bound pair
Onset at
Phonon creation is necessary
Much lower absorption coefficient than direct Semiconductors
Characteristic “Shoulders” instead of absorption lines!
None-Zero kinetic energy

## Slide 6: Direct bandgap: Resonant luminescence of free exciton-polaritons
The emission spectrum different from the absorption spectrum
Reabsorption of the emitted photon and generation of a new exciton
Electronic-polarization and optical wave mix and propagate: exciton-polariton
Longitudinal transvers splitting (), lifted degeneracy due to the interaction
High donor concentration leads to the occurrence of the “UPB/LPB Dublets”

## Slide 7: Direct bandgap: Luminescence of free excitons with emission of optical phonons
Relatively high intensities, despite the participation of a third quasi-particle
  Luminescence photon energy lowered by , so less reabsorption and scattering
  Phonon emission facilitates the radiative recombination of all the free excitons residing at LPB.
The emission lines should reflect both:
  “Maxwell-Boltzmann” distribution of free exciton kinetic energy
  Probability of phonon creation

## Slide 8: Luminescence of free excitons in indirect-bandgap semiconductors
No polariton state
Phonon emmission with is necessary
But unlike direct-band gap
The line shapes exactly reflect “Maxwell-Boltzmann” distribution of exciton kinetic energy

## Slide 9: Bound excitons
Localized at traps like dopants or residual impurities
Higher luminescence efficiency than that of FE.
  Large radius of Wannier exciton () and large capture cross section ()
      is comparable to (radiative recombination life time in direct semiconductors)
      The chance of free excitons to recombine is roughly the same as the BE!
  “Giant oscillator strength”:
    Contribution of all the unit cells inside a volume () around a defect
How to find?
  Very narrow lines which do not broaden with temperature