## Slide 1: Disordered semiconductors, Stimulated emission
Mahtab Sangghaleh- 19 Nov. 2012

## Slide 2: Luminescence of disordered semiconductors
Disordered semiconductor (amorphous) No order in atomic arranagement
e/h wavevector k, Bloch theorem, E=E(k): shouldn’t be used
Cunduction/Valenece bands, forbidden gap and density of states are conserved

## Slide 3: Densities of states in bands
(mobility edge) Free electrons
Spatially localized in traps
Charge transport: through hopping mechanism/multiple
trapping
Differing in bond lengths/angles from crystalline lattice
Energy bandgap in crystalline semicondutors
Correlation energy

## Slide 4
Nonequilibrium e-h pairs (generation rate G)
Thermalize (ps) toward mobility edges
Fall down into tail states
Tunneling between neibouring
States radiative recombination
(longer time scale)
Disordered semiconductors: radiative and non-radiative recomibinations

## Slide 5
Deflected covalent bonds in Neighbouring atoms
Mechanical strain
Dangling or
Unsaturated bonds
unpassivated bonds (ex. Through Hydrogen
passivation like a-Si:H) introduce deep localized
electron states in the middle of the BG- non-radiative centers
Disordered semiconductors: radiative and non-radiative recomibinations

## Slide 6
Probability of
thermal excitation
Frequency factor:
characterizes
The width of the
tail states
Temperature effect on luminescence

## Slide 7
Distribution of luminescence lifetime
Large life time range (between )
Tail states are broad and have variable spatial density
Probabality of the radiative tunneling
Where R is separation between localized
electron and localized hole
Continuous distribution of luminescence
decay times
Because of the considerable width it is plotted
a function of logarithmic decy time

## Slide 8
Distribution of luminescence lifetime
Number of excited centers
Laplace transform

## Slide 9
In materials with large tail state widths
The luminescence is present at RT
Distribution of luminescence lifetime

## Slide 10
Spectral shape of the emission band
PL emission spectra of pure amorphous
Semiconductors, FWHM: 200-400 meV
To explain spectral shape:
Free e-h pairs ×
Radiative recombiantion type or ×
EHL and EHP ×
Electron-phonon coupling √
Broad emissin band of a-Si:H
Phonon broadening model
Large Huang-Rhys factor S>>1
Emission peak: 1.4 eV
Band width: 1.9 eV
Shift:
Assumption of fixed value of no-phonon energy
Not symmetric emission band
Spectral shape
No-phonon energy

## Slide 11
Opposite approach: disordered broadening by Boulitrop & Dunstan
Tail states: solid (without electron-phonon interaction)
Sizeable emission band width: wide distribution of tail states
Similar approach to free e-h pairs model in indirect bandgap:
convolution of occupied e-h states in the relevant tails states
Distribution function of carriers recombine radiatively in the
tail states ×
Spectral shape of the emission band
Fast thermalization of non-equilibrium carriers down to the
lower states within a critical valume before recombination
Critical volume, driven by rate of hopping carrier diffusion (non-
Radiative tunnelling transitions to lower unoccupied states)
Reference e-h pair
N other
couples
of states
Shape of emission specta (holds for a singel value of )

## Slide 12
Spectral shape of the emission band
For a-Si:H
Unlike the recombination of free e-h pair in indirect BG
Here there is no arbitrary recombination
Values of occupied tail states densities
Comparision theoretical lineshape with
Two experimental spectra
Calculaetd spectra narrower than measured spectra
Curve d: taking inot account experimental distribution
function of radiative lifetimes with zero-phonon width
(wider but still narrower than the experimental curves)
To improve disordered broadening model
exsictance of the hot luminescence

## Slide 13
Some properties of luminescence of disordered semiconductors
Correlation effects
Non-radiative recombination
Luminescence of impurities and defects
Luminescence ’fatigue’
Correlation effects
Non-radiative recombination
Luminescence of impurities and defects
Luminescence ’fatigue’
No Wannier exciton but
Geminate: Electron and hole couple created by the absorption of a given photon in a given site
Non-geminate: Electron and a hole that have originated in different parts of the sample as a
consequence of two absorption events
Photocarrier diffusion length are short:
Low excitations: Geminate pair recombination are dominates
High exciations: Non-geminate recombination is not negligible
Controversial discussion:
Radiative recombination takes place in arbitrary pairs or geminate pairs only?!
No injection EL in amorphous (all the electron hole pairs non-geminate)
In a-Si:H p-i-n low intensity EL
Proves non-radiative recobination of non-geminate e-h pairs

## Slide 14
Correlation effects
Non-radiative recombination
Luminescence of impurities and defects
Luminescence ’fatigue’
Some properties of luminescence of disordered semiconductors
Possible paths of non-radiative recombination of
e-h pairs in amorphous ssemiconductors:
Recombination mediated by dangling bonds
(Shotckey-Read recombination of defects in
the middle of the bandgap
Thermal quenching
Recombination of non-radiative e-h pairs
Auger recombination
Surface recombination
Stachowitz et. al.
Non-radiative recombionation due to non-geminate e-h pairs
Small-radius localized exciton
Two maxima in lifetime distribution: singlet & triplet excitons
Reconciled with existence of EL

## Slide 15
Correlation effects
Non-radiative recombination
Luminescence of impurities and defects
Luminescence ’fatigue’
Some properties of luminescence of disordered semiconductors
Surface recombination in thin surface layers: Unsaturated bonds near the surface
Thickness of non-luminescence layer
D Photocarrier diffusion coefficient (small in disordered semiconductors )
Although the concentration of surface defect is high , small contribuion in surface
non-radiative recombination (~ 10%)

## Slide 16
Correlation effects
Non-radiative recombination
Luminescence of impurities and defects
Luminescence ’fatigue’
Some properties of luminescence of disordered semiconductors
Distribution of binding energies
Impurities: new dangling bonds
Mainly non-radiative
High doping: weak luminescence
a-Si:H doped with phosphorus/boron
new emission band in Infrared ( ~ 0.8 eV)
Why radiative processes like
Hasn’t been observed in amorphous
Semiconductors?

## Slide 17
Correlation effects
Non-radiative recombination
Luminescence of impurities and defects
Luminescence ’fatigue’
Some properties of luminescence of disordered semiconductors
Gradual fading of main emission band under
high excitation
Staebler-Wronski or light- induced formation

## Slide 18: Stimulated emission
Special case of luminescence
Different thermodynamic conditions needed for occurance
Polpulation inversion
Need to be based on different principles

## Slide 19
Spontaneous versus stimulated emission
Fundumental principle of lasers √
Basic resseach on radiative recombination ×
Shape of the sample and the applied
geometery of experiment
Large excited spot (~ 1mm) and high optical quality
surface: spontaneous emission will stimulate the
emission of other photons
Decreasing excited spot leads to suppression of
stimulated emission, new M line due to radiative decay
Of excitonic emission
High excitation/ excited area

## Slide 20
Spontaneous versus stimulated emission
Decay time of stimulated emission is much faster than
spontaneous emission
Rate of transitios from I2> to I1> by spontaneous emission:
( Einstein coefficient )
Rate of stimulated emission from I2> to I1> (or vice versa):
and
specral energy density of resonance radiation
Einestein coeficient of absorption and stimulated emission

## Slide 21
Absorption coeeficient
Population of individual levels: N
Density of optical transition: p
Introduction of
Lineshape function
Parallel beam of photons with power flux density (Intensity)
Impinging to the atomic system in the z-direction
Intensity variation
Contribution of spontaneous emission in given direction is much smaller than stimulated emission
For non-degenerate levels
Lambert-beer law satisfied

## Slide 22
Optical gain
Nonlinear character of stimulated emission: it’s emission line shape is dependant on the
intensity of stimulating light
Spontaneous and stimulated emission occurs simultaneously in luminescence experiments
Density of states in the conduction and valence band
We had this (for band-to-bad spontaneous
emission under low excitation
f(v): probabilty of ’suitable occupancy states’
Occupied joint states per unit volume: to emit 1 photon
Light with a broad spectral distribution: u(v)

## Slide 23
Optical gain
Probability density of stimulated emission
(Stimulated emission rate (the number of the photons) emitted per 1Hz & 1cm˄3)
The overall stimulated emission rate
Linewidth of energy levels in semiconductor is much smaller than the frequency band of
stimulated emission, approximation:
I(v) should satisfy Lambert-beer law
Spectral distribution of the intensity
Occupancy condition for absorption
The role of the probe beam in luminescence experiment taken on by spontaneous emission in a given direction

## Slide 24
Optical gain
Light wavelength in vacuum
n refractive index
The specral shape of gainis influenced by occupancy of electron states in conduction band and hole states in valence band (Fermi inversion factor) or the pump intensity
Experiment: detected emission spectra: Both spontaneous & stimulated with overall radiative life
Relative part of the excited volume of material that takes part into stimulated emission

## Slide 25
Spectral shape of the optical gain
Separate quasi-Fermi level for electrons/holes
Fermi inversion factor
Condition for the occurance of optical gain in semiconductors
Bernard-Duraffourg condition for inverse population of states for
a degenerate semiconductor
Inversion population in atomic levels:
In quasi-continua states:
Amplification of light through stimulated emission in semiconductors occurs only for photons arise from radiative transitions between states in CB with probabilty of being occupied by electrons larger than ½, and states in VB with the probability of being occupied by electrons lower than ½.

## Slide 26
Spectral shape of the optical gain

## Slide 27
Spectral shape of the optical gain
More precise calculation of Gain:
Transition Matrix
Numerical factor (effective mass-several VBs)
EHP: Ignoring k-conservation law
Inhomogeneousely distributed e-h pairs distorts the ideal translational symmetry of the lattice
The presence of impurity atoms
Radiative EHP recombination k conservation is hold locally through multiple collisions between electrons & holes

## Slide 28
Spectral shape of the optical gain
High concentration of e-h pairs: relaxation of k conservation
Naturally: Gain would depend on pumping intensity
At transitions to negative gains: have to change to square root dependence
Experiment observation: Not consistent
Doping of the semiconductors
For highly impure semiconductors the characteristic shape of the gain shouldn’t be observed
which is not true in experiment
Gentel Increase of gain close to (instead of square root dependance) and overall asymmetry of the gain curve: two corrections factors
Final state damping in EHP
Excitonic enhancement
Dashed lines: theory calculations, considering k-conservation law and
Final states damping and excitonic enhancement

## Slide 29
Spectral shape of the optical gain
Spectral position of the gain with respect to the maximum of the spontaneous emission band
The effect of temperature on gain
The frequency factor in gain shape
The higher the temperature more difficult:
Factor enhances gain curve magnitude, more pronounced at low frequencies

## Slide 30
Stimulated emission in indirect bandgap semiconductors
Longer radiative recombination, lower values of optical gain
Free carrier absorption (FCA): Drude model
Free electron gas with free electron concentration
Optical radiation frequency
Imaginary part of dielectric constant

## Slide 31
Stimulated emission in indirect bandgap semiconductors

## Slide 32
Experimental techniques for measuring the optical gain
Variable stripe length (VSL) technique
Pump and Probe method (P&P)
- Both techniques are based on direct measurements of the amplification of a weak probe beam
Difference: methods in the origin of probe beam

## Slide 33
VSL technique
FCA
Impurities
Increase of stripe
length dx
Solution
Mode confinement factor
Modal gain
g(v) is material gain

## Slide 34
VSL technique
High optical gain in 1970’s
Deviation between fitted line with
experimental data gets shorter with increasing excitation intensity: Gain saturation
Spectral narrowing by increase of l
High gain value
Low gain values, VLS is less reliable

## Slide 35
VSL technique
In the case
Several parameters should be considered:
If t is too large
Const. pump intensity along stripe:
rectangular beam profile & uniformly
distributed pump energy
Part of Gaussian beam can be used
Constant efficiency of coupling of I(SPE)
to monochromator or detector
Diffraction of the pump beam on the slit
or razor blade, limiting utilization of the
stripe length

## Slide 36
Pump and probe method (P&P)
Weak external probe beam
Changes in the absorption coefficient
of the probe beam