## Slide 1: Luminescence of excitons and Highly excited semiconductors
Federico Pevere
Ph.D. student
Materials and Nano Physics Department
ICT school, KTH Royal Institute of technology
Notes: Good morning to everyone, I am Federico Pevere and today I will talk you about the luminescence of excitons and I will also explain you what happens in highly excited semiconductors.

## Slide 2: Outline
Luminescence of excitons
  Wannier exciton
  Bound excitons
Highly excited semiconductors
  Biexciton
  Collisions of free excitons
  Electron-hole liquid (EHL)
  Electron-hole plasma (EHP)
  Bose-Einstein condensation of excitons
Notes: This is the outline of my presentation: POINT TO THE SLIDE

## Slide 3: Luminescence of excitons

## Slide 4: Exciton
Exciton: bound (via Coulomb forces) electron-hole pair
exciton internal energy < Eg
quasi-particle representing the lowest electronic excitation in a semiconductor
1. Frenkel exciton (molecular crystals):
localized at a specific atom/molecule
moving through the crystal by hopping
2. Charge transfer exciton (ionic crystals):
electron transfer from anion (-) to cation (+)
3. Wannier exciton (semiconductors):
electron and hole separated over many lattice constants
exciton wavefunction highly delocalized => free exciton
Notes: To begin with, an exciton is a quasi-particle consisting of an electron and a hole bound together via Coulomb forces. Its internal energy, due to the Coulomb attraction, is less than the bandgap energy of the corresponding semiconductor. The exciton is the lowest electronic excitation in a semiconductor.
There are three types of excitons: Frenkel excitons occur in molecular crystals, they are localized at a specific atom or molecule and they move through the crystal by a hopping mechanism. Charge transfer exciton are typical of ionic crystals. In Wannier excitons, also called free excitons, electron and hole are separated over many lattice constants. The exciton wavefunction is thus strongly delocalized and the exciton can move freely inside the crystal. This kind of exciton occurs mainly in semiconductors.

## Slide 5: Wannier exciton
modified Bohr model of the hydrogen atom
Typical values for a semiconductor:
, =>
Total exciton energy:
Centre of mass: free particle, , (for optically generated excitons)
Relative motion: it behaves like a donor,
crystal
1
2
Notes: By applying a modified model of the hydrogen atom, we can find the electron orbits that are expressed by this equation where: epsilon is the dielectric constant of the crystal, mr is the exciton reduced mass, m0 is the free electron mass, n is the principal quantum orbit number and aB is the Bohr radius of the hydrogen atom. For a typical semiconductor, the exciton ground state radius is approximately 5 nm. To find the exciton energy we can decompose the motion of the exciton in the centre of mass motion, which is represented by a mass equals to the sum of the electron and hole effective masses and behaves like a free particle, and the relative motion which behaves like a donor. In the figure (b) you can see the dispersion relation of a free exciton. Notice that for optically created excitons the quasi-momentum of the centre of mass is approximately 0.

## Slide 6: Wannier exciton
Binding energy (, ) of the order of tens of meV
at
=> excitons in semiconductors occur only at low T
Impurity atoms represent very efficient traps for the free excitons propagating through the crystal
=> if the crystal is not pure, bound excitons are created
Notes: Since the Wannier exciton binding energy of the ground state is of the order of tens of meV, at room temperature the collisions with phonons can lead to the break if the bound between the electron and the hole. Hence, free excitons are only observed at low temperatures and in pure crystals, in fact impurities can trap the excitons giving a bound exciton

## Slide 7: Absorption spectrum of Wannier exciton
Distinctive absorption lines at
Intensity
Optical absorption enhanced for
Direct bandgap semiconductor
Indirect bandgap semiconductor
Exciton created with a minimum energy has
=> phonon (ℏω)
Threshold energy shifted to
No absorption lines
Notes: Let us consider a direct bandgap semiconductor first. If we measure the absorption, we can clearly see that the behaviour doesn´t follow the one here shown by the dashed line that doesn´t consider any excitonic effect. Instead, we have distinctive absorption lines, each one corresponding to a excitonic state whose intensity is proportional to 1 over n cubic. For a photon energy greater than the bandgap the optical absorption is enhanced thanks to the excitons.
For an indirect semiconductor, a participation of a phonon is required, due to momentum conservation, in order to form an exciton. In this case, the threshold is higher and there are not absorption lines, just so-called ”shoulders”.

## Slide 8: Resonant luminescence of exciton-polaritons
Mixed electronic-polarization and optical wave propagating through the lattice => exciton-polariton
Upper (Lower) polariton branch, referred as UPB (LPB)
No-phonon luminescence near , two emission lines separated by
Notes: In the emission process of a direct bandgap semic., the interaction between excitons and photons cannot be neglected and leads to the so-called exciton-polariton. The resulting curve is shown in Fig.(b): as we can see, there are two branches UPB and LPB separated by the so-called bottleneck.
If polaritons are created via non-resonantly absorption of photons with energy above the bandgap, as for example in Fig.(C) in point A, they will thermalize fast emitting optical and acoustic phonons and, after their lifetime they will recombine giving rise to a no-phonon exciton-polariton luminescence consisted of two spectral lines corresponding to the two branches.

## Slide 9: Resonant luminescence of exciton-polaritons
UPB/LPB doublet affected by the concentration of residual impurities, particularly donors (Koteles et al.)
Two cases:
No impurities: just LPB branch
High concentration of donors: UPB and LPB due to elastic scattering of exciton-polaritons with donors (hole-burning)
Photoluminescence assesment method used even in microelectronics industry
Notes: It has been noticed that the occurrence of the UPB/LPB is affected by residual impurities, particularly donors. After thermalization, all the exciton accumulate just on the LPB branch and, accordingly, they should give rise to just a single spectral line. However, when high donor concentrations are present, the exciton-polaritons are scattered by donors and this scattering leads to the emergence of the doublet.

## Slide 10: Luminescence of free excitons with emission of optical phonons
significant especially in II-VI semiconductors
spectral position at
lines marked as X-LO, X-2LO, etc.
intensity relatively high => ???
Notes: In direct-bandgap semiconductors, particularly in II-VI type, luminescence with simultaneous emission of LO-phonons (TO-phonons too) is quite significant. For energy conservation, the spectral position are at POINT FINGER TO THE SLIDE. These lines are marked as … and they intensity is quite high even though they result from a process which involves participation of a third quasi-particle which we would expect to be less likely to happen…

## Slide 11: Luminescence of free excitons with emission of optical phonons
high-intensity X-LO and X-2LO because:
  photon energy is lowered by => no resonant polariton complications (reabsorption and scattering)
  only zero-wavevector (i.e. zero kinetic energy) polaritons can undergo resonant no-phonon recombination
  with phonons, all free excitons can take part in the radiative recombination process
lineshape:
Probability of phonon creation
Notes: However, the intensity is high because: 1st the lowering of the photon energy avoids complications of the resonance (reabsorption and scattering) 2nd all the free excitons, not just those with Ek=0 in the no-phonon emission, can participate in the radiative recombination process. From the lineshape formula one can notice that a new term appears, the probability of phonon creation.

## Slide 12: Luminescence of free excitons with emission of optical phonons
Probability of phonon creation:
  X-LO (m=1):
=>
  X-2LO (m=2):
  =>
Notes: In the case of one-phonon creation, since the modulus of the phonon wavevector must be almost equal to that of the exciton, the probability goes like the exciton energy, whereas for two phonons the probability is independent on the exciton wavevector and it is constant. Notice that acoustic phonons have low energy at low values of wavevector qphonon, therefore they cannot release photons from the bottleneck region (i.e. they cannot enable photons to escape from resonant reabsorption).

## Slide 13: Luminescence of free excitons with emission of optical phonons
Participation of optical phonons in free exciton radiative recombination in direct bandgap semiconductors:
removes polariton effects
Fröhlich coupling: these phonons have strongest coupling in polar semiconductors (particularly in II-VI materials)

## Slide 14: Luminescence of excitons in indirect bandgap semiconductors
Absence of polariton states (non-crossing exciton and photon dispersion curves)
indispensability of phonon participation in radiative recombination process
Notes: In indirect bandgap semiconductors the first thing we notice is the absence of polariton states. The participation of phonons to the radiative recombination process here becomes fundamental. Moreoever, the probability of phonon creation does not depend on qphonon, thus the lineshape reflects Maxwell-Boltzmann distribution of exciton kinetic energies.

## Slide 15: Luminescence of excitons in indirect bandgap semiconductors
Si and Ge:
Si: TA-, LO- and TO- replicas are observed, the weak LA-line merges with the LO-line
Ge: allowed LA- and TO- replicas are observed
SELECTION RULES
IMPOSED BY CRYSTAL SYMMETRY APPLY!

## Slide 16: Bound excitons
Trapped in potential wells created by impurity atoms
Extrinsic luminescence
Efficiency of their luminescence higher than FE
  Large radius of Wannier exciton => large capture cross-section
  All the unit cells inside around the impurity atom or defect contribute to radiative recombination of the bound exciton
Mean exciton lifetime
before trapping
: exciton capture cross-section
: impurity concentration
: thermal velocity of exciton diffusion through the lattice

## Slide 17: Bound excitons
Typical values for a semiconductor:
(nominally pure semiconductor, except Si)
(i.e. )
Direct bandgap
Indirect bandgap

## Slide 18: Excitons bound to shallow impurities
1. Excitons bound to ionized donors (D+-X) or acceptors (A--X)
Using quantum-chemistry notation:
Emission of a photon :
Energy separation between the low-energy threshold of the free exciton line and the maximum of the bound exciton line = binding energy
Binding energy
of the exciton
in the relevant complex

## Slide 19: Excitons bound to shallow impurities
1. Excitons bound to ionized donors (D+-X) or acceptors (A--X)
Restrictions on for the complex to be stable
D+-X and A--X cannot exist simultaneously
A--X very unlikely
Si () no excitons bound to ionized impurities at all
GaAs () and InP () have => D+-X exists
Notes: The kinetic energy of the second particle should be low, there is a critical value of sigma for the complex to be stable.

## Slide 20: Excitons bound to shallow impurities
2. Excitons bound to neutral donors/acceptors
Stable at an arbitrary ratio
Heavy hole limit : analogous to H2
  Dissociation energy of H2 =
  By analogy, with donor ionization energy
Light hole limit : analogous to H- ion
  Dissociation energy of H- =
  By analogy, with donor ionization energy
CREATION:
RADIATIVE DECAY:

## Slide 21: Excitons bound to shallow impurities
2. Excitons bound to neutral donors/acceptors
Emission of bound exciton is red-shifted by
Relation between and is material-dependent

## Slide 22: Excitons bound to shallow impurities
2. Excitons bound to neutral donors/acceptors
Hayne´s rule (donor case) :
Explained theoretically through chemical shift of the short range potential
Inapplicable to some II-V compounds and validity not accepted in II-VI semiconductors
GaP:

## Slide 23: Excitons bound to shallow impurities
3. Bound multiexciton complexes (BMEC)
Discovered in 1970s by Kaminskii and Pokrovskii, theoretically unexpected
BMEC: 1, 2, 3 or more excitons with dimishing binding energies are successively wrapped around D0 or A0, they later annihilate radiatevely
m BE: energy of the mth bound exciton
1 BE = (D0-X)

## Slide 24: Excitons bound to shallow impurities
3. Bound multiexciton complexes (BMEC)
Radiative decay of the mth exciton: +

## Slide 25: Excitons bound to shallow impurities
3. Bound multiexciton complexes (BMEC)
Radiative decay of the mth exciton: +

## Slide 26: Excitons bound to shallow impurities
3. Bound multiexciton complexes (BMEC)
New lines due to energy level splitting
BMEC occur mainly in indirect bandgap semic.
  long exciton lifetime => likely than more excitons are present at one centre
  N-fold degenracy of the conduction band minimum (2N electrons can be placed)

## Slide 27: Excitons bound to shallow impurities
Low-T PL spectroscopy is used to determine the concentration of shallow donors and acceptors in crystalline Si
TO-replicas are used for the quantitative analysis
Spectral positions of donors/acceptors varying according to Hayne´s rule, they are distinguishable
Limits of applicability:
Necessary to choose optimal level of cw pumping
Fourier luminescence spectroscopy (higher S/N, better accuracy)
Insufficient cooling leads to rapid deterioration of the measurement sensitivity
Efforts to extend PL diagnostics of dopants to other semiconductors
Notes: TO lines are chosen because in their spectral range both lines originating from BE and FE are relatevely intense. No pulsed lasers due to EHL luminescence, limits of applicability due to low intensity of BE lines at low doping concentrations and low intensity of FE lines at high doping concentrations. A difference of just 3 K in temperature can lead to an intensity ratio BTO(BE)/ITO(FE) decreased by more than one order of magnitude!

## Slide 28: Excitons bound to isoelectronic impurities
Exciton can be trapped at isovalent or isoelectronic impurities
impurities belonging to the same group (column) of the periodic table of elements of the original consituent
Examples: GaP/N, AgBr/I-
Highly efficient channel of radiative recombination
Physical mechanism based on electronegativity X:
  XN=3.0>XP (captured photoelectron)
  XI=2.7<XBr (captured photohole)

## Slide 29: Excitons bound to isoelectronic impurities
Localized excitation => use of configurational model
can vary according to the strength of exciton-phonon interaction (Huang-Rhys factor, S)
  GaP: => sharp emission line
  AgBr: => broad emission line
For AgBr (single I- ion per approximately
107 ions of the host lattice):
Enhancement factor:
Notes: A line originates from exciton J=1, B line from J=2. Splitting caused by electron-hole exchange interaction (singlet and triplet exciton terms are used). The term zef, representing the enhancement factor is very high considering the iodine concentration in the host lattice.

## Slide 30: Excitons bound to isoelectronic impurities
High-intensity due to absence of Auger recombination (3rd quasi particle missing)
Strong localization in real spac leads to:
  strong delocalization in k space (Heisenberg uncertainty principle)
  quasi-direct radiative recombination
Green-emitting EL diodes based on GaP/N
Notes: Gree-emitting diodesm arrow indicate position of lines that merge together at 300 K. Percentages indicate GaN content.

## Slide 31: Self-trapped excitons
In polar semiconductors with strong exciton-phonon interaction
Intrinsic luminescence process
Phenomenological description by Toyozawa
Two exciton states: free (F) and self-trapped (S)
Self-trapped exciton: localized in a potential well due to strong lattice deformation around it
Phase diagram for deformable lattice
  B: total energy width of exciton band
  ELRl: lattice-relaxation energy, long-range
  ELRs: lattice-relaxation energy, short-range
No self-trapping in IV, III-V and II-VI semic.

## Slide 32: Self-trapped excitons
AgCl:
  Q is the separation of Cl- ligands from the central Ag2+ ion in (AgCl6)4-
  Δ (≈5 meV) is the potential barrier that must be overcome by excitons to reach state S => free exciton stays in F minimum only for a very short time
  Time to overcome barrier ≈ 70 ps

## Slide 33: Highly excited semiconductors

## Slide 34: Highly excited semiconductors
Excitation intensity increased to -
Use of pulsed lasers
Emission spectrum: new lines or bands appear

## Slide 35: Experimental considerations
In steady-state conditions (Hp: homogeneous exciton density at one-photon excitation):
Typical case (direct semiconductor):
,
the mean interexciton separation is
no interaction between excitons!!!
In order to have interaction:

## Slide 36: Experimental considerations
In reality:
  Concentration gradient pushes excitons from subsurface layer (thickness ) deeper into the sample reducing their concentration
  Efficient non-radiateve recombination of exciton at surface states
  from up to
Superiority of two-photon excitation where is valid and
!
=> We are close to the threshold of sample destruction!!!

## Slide 37: Excitonic molecule (EM) or Biexciton
Free biexciton: quasi-particle (2e,2h) propagating freely through the crystal lattice
For typical semiconductors ():
  EM less resistant to thermal dissociation than FE => liquid-He cryostat
Radiative recombination of EM:
  one of the excitons undergoes a transition to the free exciton
  the second exciton recombines, emitting a photon => novel emission line!

## Slide 38: Identification of the EM emission line
We have to analyse:
  Lineshape
  Intensity dependence
  Spectral position
  Temperature behaviour

## Slide 39: EM lineshape in direct-bandgap semic.
Formation of biexciton:
EM Radiative decay (1 photon + 1 exciton):
Lineshape (inverse Maxwell-Boltzmann distribution):
Exciton
Exciton
Biexciton
2
Notes: Two exciton of energy Eg-EX fuse together to form a biexciton with the simultaneous release of binding energy EB. The emission line is shifted with respect to the position of the free exciton absorption line (Eg-EX) by EB towards low photon energies. As you can see, the biexciton effective mass is higher than the exciton effective mass => asymmetric lineshape with a low energy tail. NB occupation probability of the upper (biexciton) level is given by the Boltzmann factor. For the radiative recombination, both energy and quasi-momentum conservation are applied. In the biexciton case all the biexciton, independently of their wavevector, participate in the radiative dacay.

## Slide 40: EM lineshape in direct-bandgap semic.
All biexcitons (i.e. all ) are supposed to take part in the radiative decay
Biexciton momentum is carried away by the so-called recoil exciton (released):
=> momentum always conserved
Polariton effects can be neglected
Biexciton luminescence can become a very efficient channel of radiative recombination in highly excited semiconductors
Notes: EM emission can take part even in stimulated emission.
Fig (a): CuCl, solid curve experimental data, dashed curve theoretical data. TM=18K, EB=28meV, each line corresponds to exciton state (longitudinal and transverse, deltaLT=5meV). Pex=4.8kW/cm^2. Increase in Pex or TM leads to biexciton collisions=>lineshape more symmetric.
Fig (b): indirect bandgap semic. ...

## Slide 41: EM lineshape in indirect-bandgap semic.
Exciton band located at biexciton band located at
  Phonon participation is required
Downwards transitions from give photons
  maximum photon energies, in all other transitions lower photon energies
  Higher broader high-energy edge ()
Entire population of EM participating in luminescence process
Notes: In this case the participation of phonons is required in order to have momentum conservation. However, the lineshape doesn´t change from the direct-bandgap case.

## Slide 42: EM lineshape in indirect-bandgap semic.
Biexciton emission line (similar to inverse of Maxwell-Boltzmann distr.):
Cho has proposed a matrix element of the form:
  stands for biexciton radius: it is crucial factor for the lineshape!!!
Notes: aM is biexciton radius (average separation of the two holes in a biexciton). Physical background : M drops rapidily from its maximum at KM=2KX down to almost zero just for |KM/2-KX| approx aM^-1. aM crucial factor driving emission lineshape. If we come back to the fig (b) we can see the two lines: excitonic line and biexcitonic line (both with emission of TO-phonon).

## Slide 43: M-line intensity dependence
Important auxiliary guideline for firm identification of EM emission line
Intuitively quadratic, experimentally with on average
Knox explanation:
  Simultaneous monomolecular and bimolecular processes
  ´optical´ and ´thermal´ excitons
  M-line intensity dependence:
    : characteristic material-dependent excitation intensity
Notes: Biexcitons can be created by fusing ´thermal´ excitons only.

## Slide 44: Determination of EM-parameters
Two modes of assessing EB :
  Spectroscopic
  Thermodynamic:
    Sample heating: EM dissociates more easily than FE (EB<EX)
    Intensity ratio is driven by
    Semi-logarithmic plot of against
      Slope gives (1.53 meV for Si, spectroscopic value 1.46 meV)
Radius aM:
  indirect semiconductor: fitting with theoretical model
Notes: In addition biexcitons can get localized close to impurity centers and form bound (localized) biexcitons. Properties analogous to other extrinsic radiative channels (symmetric shape, non-dependent on intensity or temperature, line with saturation behaviour).

## Slide 45: Collisions of free excitons
2 free excitons  photon + free e-h pair
line: high-energy threshold and asymmetric
Qualitatively:
  Fusion into EM will prevail at low and large
  High concentration of FE with non-equilibrium excess kinetic energy (optical excitons)
   collisions of free excitons

## Slide 46: Electron-hole liquid (EHL)
Condensation of excitons into a Fermi liquid
  Free fermions, electrons and holes
  Similarly to classical case, electron-hole drops (EHD)
Phase diagram
EHL ground-state energy
per e-h pair
Binding energy of the condensate w.r.t. free excitons
Notes: nC and TC are the critical concentration and the critical temperature, respectively. For the EHL to be stable, it is required phi>0.

## Slide 47: EHL parameters
e-h correlation
  Probability of radiative recombination enhanced w.r.t. system of free carriers
Broad emission spectrum
  Conditions: high pumping, T<TC
Lineshape:
 recombination radiation inside drops
not absorbed in the lattice!
Reduced bandgap
Fermi-Dirac distrib.

## Slide 48: Determination of Eg’ and µ
Emission spectrum starts at and terminates at
PL unique method for direct determination of and
extraction of n0 (next slide)
Notes: See also the figure in the previous slide.

## Slide 49: Determination of n0 and φ
n0:
T=0 K:
  Full width of EHL band:
T≠0 K: numerical integration to be performed
Φ (binding energy):
µ’ spectroscopic energy relevant to EHL ground state
  Recombination from Fermi levels leaves EHL in its ground state

## Slide 50: Identification of EHL band
If increases  EHL keeps its shape and position
If increases  high-energy edge broadens, FHWM gets narrower  decreasing function of
EHL band appears upon reaching intensity threshold and disappears sharply upon reaching temperature threshold

## Slide 51: Coexistence of EM with EHL

## Slide 52: Electron-hole plasma (EHP)
(free e-h concentration)
  When (Mott density): bound e-h pairs cease to exist
Screening potential:
  screening length
When excitons become unstable:
    EHP: from gas of bosons to plasma governed by Fermi statistics
    Mott insulator-metal transition (gradual)
    EHP radiative recomb. may lead to stimulated emission
GAP SHRINKAGE
for

## Slide 53: Bose-Einstein condensation of excitons
Exciton is a boson ()  at high densities can undergo Bose-Einstein condensation
  An ensemble of bosons may always contain only a finite number of particles (dependent on )
  If we add more particles, the excess particles must ‘condensate’ to the ground state
Emission spectrum: we expect a very narrow peak on the low-energy edge of free exciton line
Till now, no unambiguous experimental evidence of Bose-Einstein condensation