## Slide 1: Electronic structure and luminescence of low-dimensional semiconductors
By Carl Reuterskiöld Hedlund

## Slide 2: Outline
Introduction
Basic types of low-dimensional semiconductors
Density of states in low-dimensional semiconductors
Quantum wells. Two-dimensional semiconductors
Quantum wires
Quantum dots
Exiton-phonon interaction. Phonon bottleneck
Special phenomena of low-dimentional semiconductors

## Slide 3: Introduction
If Crystal dimensions ~ Exciton Bohr radius = Quantum confinement which means the kinetic energy of an exciton gets quantised to discrete states
Enables band gap engineering
http://www.tf.uni-kiel.de/matwis/amat/semi_en/kap_5/illustr/exciton_bandgap.gif

## Slide 4: Basic types of low-dimensional semiconductors
2D structure = quantum well
1D structure = quantum wire
0D structure = quantum dot
Confined in 3 dimensions = quantum dot
Confined in 2 dimensions = quantum wire
Confined in 1 dimensions = quantum well
Nanowire has no quantum confinement

## Slide 5: Production of low-dimentional semiconductors
Bottom up or top down approach
Bottom up: desiered structure is deposited from precursors and stopped at an appropriate time.
Top down: Material is removed selectivly for wanted structure. Often via lithografy.

## Slide 6: Semiconductor hetrostructures
Low dimensional semiconduccotrs often contain multiple materials for several reasons:
Passivation and protection
Making it a suitable size for manipulation
Achieving appropriate energy structure

## Slide 7: Semiconductor hetrostructures
With techniques such as MBE, LPE, MOCVD and MOVPE growth of almost any semiconductor can be achieved
Lattice matched
Low strain
DBR super lattice

## Slide 8: Basic types of quantum-well hetrostructures
Estimate Band alignment by Anderson’s rule:
The vacuum levels of the material most align

## Slide 9: Basic types of quantum-well hetrostructures

## Slide 10: Density of states in a low-dimensional
K Plane wave
Probability to find particle in dV
K = Integrate over hole system
Volyms , ,
Particle in a box
)

## Slide 11: Density of states in a low-dimensional
DOS for electron in conduction band
d=1,
d=2,
d=3,

## Slide 12: Quantum well with infinite barriers
Infinite in xy plane and thickness in z plane
V(z) = 0 for –(/2) < z < (
V(z) = for |z| > (
Solving the Schrödinger equation yields the wave function and its energy
(z)=, =, =1, 2, 3, …
(z)=, =, =1, 2, 3, …

## Slide 13: Quantum well with infinite barriers
E==(+) j=1, 2 , 3, …
)=)

## Slide 14: Quantum well with finite barriers
V(z) = 0 for –(/2) < z < (
V(z) = for |z| > (
Solving – (–) )=0
Yields )=
To simplify we introduce:
and

## Slide 15: Quantum well with finite barriers
We get the simple form:
tan()=
Odd solutions:
-cotan()=
Example of =12nm GaAs QW with =0.3eV
The number of possible localized states is limited by

## Slide 16: Quantum well with finite barriers
The higher the energy state the bigger the evanescent wave in the barrier

## Slide 17: Excitons in a quantum well
, =
This means the 2D exciton binding energy increases and decreases() which means the electron-hole binding interaction increases
, =
The oscillator strength of a 2D crystal is much higher compared two its bulk value
it drops rapidly with higher states which tells us that higher states have a weaker optical manifestation

## Slide 18: Optical transitions in a quantum well
Blue shift with decreasing QW width
Selection rule for infinte barrier
Selection rule for finte barrier
The QW breaks the symmetry in z direction lifting the degeneracy thus seperating ligth and heavy holes

## Slide 19: Luminescence of quantum wells
Usually only the lowest energy transition can be seen in luminescence spectra because of efficient relaxation of higher into lower energy states
There is a red shift due to interface roughness. There is energy relaxation with an in homogeneously broadened band

## Slide 20: Luminescence of quantum wells
Blue shift in emission spectra from decreased QW thickness enabling measurement of thickness if composition is know or composition if thickness is known
The FWHM should be more than half that of bulk material making for example lasing easier
Luminescence works at higher temperatures due to higher exciton binding energy and more overlap of wave function
Population densities can reach very high values

## Slide 21: Luminescence of quantum wire
As spot size decrease the spectra of individual excitons can be seen

## Slide 22: Quantum wires
Are most often made by first growing the material then etching out the quantum wire
Gold is also commonly used as a nucleation site in growth to produce quantum wires
http://eng.thesaurus.rusnano.com/upload/iblock/3ae/quantum%20wire.jpg
http://www.mrc.ethz.ch/research/materials_for_communication/Ensslin_back2_left.jpg?hires

## Slide 23: Density of states in quantum wires
(E)=

## Slide 24: Optical absorption and emission of quantum wires
Absorption in the quantum wire is characterized by excitonic resonance
The quantum wire has weak confinement in one direction

## Slide 25: Quantum wire luminescence spectra
Spectral broadening due to Pauli exclusion principle

## Slide 26: Quantum dots
V(r) = 0 for r R
V(r) = for r > R
If
then =
Where is the n-th root of the l-th-order bessel function

## Slide 27: Energy levels in a infinitely deep spherical well
We have the quantum numbers n, l and m which are the principle, the orbital and the magnetic quantum numbers
The energy of the state is determined by n and l
The magnetic quantum number m can acquire (2l+1) values of 0, and this degeneracy can be lifted in an magnetic field

## Slide 28: Types of quantum dots according to the strength of the quantum confinement effect

## Slide 29: Strong quantum confinement regime
<< R <<
The absorption spectra have peaks at
=
The ground state(n=1 l=0) with Coulomb interaction taken into account
=- 1.786

## Slide 30: Strong quantum confinement regime
Taking the correlation energy into account and generalizing the exciton ground state yields
=1.7860.248
Triangles show exciton bohr radius

## Slide 31: Luminescence of quantum dots
Quantum dots can be repaired in many different ways therefore it is hard to find generally valid features
Some features they do share are:
Emission spectrum is blue shifted with decreasing size
Edge emission is superior to its bulk properties
Emission can be seen at high T
Emission and excitation spectra is broadened because of different shape and size of the quantum dots

## Slide 32: Luminescence of quantum dots
Low temperature measurement of different AgBr samples
The free exciton edge emission grows by 4 orders of magnitude
The impurity related emission completely disappears

## Slide 33: Luminescence of quantum dots
Nano crystals are placed in a solution at high temperature and grows slowly into bulk sized crystals
Absorption spectra goes from structured to smooth
Emission spectra redshifts then coulomb interaction starts to prevail and the spectra narrow into a excitonic maxima

## Slide 34: Luminescence of quantum dots
Light with different energies are used to excite different sized CdSe nanocrystals

## Slide 35: Exciton-phonon interaction, phonon bottleneck
Normally hot carriers throw away their energy through LO phonons and then acoustic phonons
In sufficiently small nanocrystals it can cool off only to the discreet energy states and the LO phonon does not have enough energy to achieve this
Only through multi-phonon LO+LA/TA emission can the hot carrier cool down

## Slide 36: Phonon bottleneck
As the size of the nanocrystal decreases the phonon interaction decreases
Or it is because of the smaller electric dipole moment of the exciton that decreases with smaller crystal i.e. weakening Frölich interaction

## Slide 37: No phonon bottleneck
Other experiments show opposite phenomena
Relaxation time decreases with shrinking quantum dot radius
Proposed solution was a new relaxation mechanism that utilizes the surface to the passivating shell(surface vibrations) this is the so called adiabatic transition

## Slide 38: No phonon bottleneck
Another mechanism for cooling of the carrier through a type off auger recombination with coulomb electron-hole interaction
The electron falls down to the bottom of the conduction band via an interband transition and via coulomb interaction transfers its energy to the hole
The hole which has more states due to band degeneracy and greater mass can cool by emitting phonons

## Slide 39: Excitons indirect in real space
A spatially separated electron and hole its overlap in wave function and combined recombination energy can be manipulated via an electric field

## Slide 40: Excitons indirect in real space
Three double GaAs quantum wells with thin AlAs barriers
When voltage is applied a noticeable redshift occurs
The shift saturates because of shielding created by a substantial amount of indirect excitons

## Slide 41: Enhanced photoluminescence intensity during measurement
A 200nm CdSe film on Si shows a 20 fold increase of intensity during exposure
Effect depends on external parameters such as atmosphere, substrate material and thickness of film
Proposed explanation is the passivation off dangling bonds (surface)

## Slide 42: Enhancement of luminescence intensity by metal nano particles
When a metal nanoparticle is in close proximity of an exited QD plasmonic oscillations in the nanoparticle. This surface plasmon then concentrates the optical field into the QD which increases the emission efficiency via Purcell effect
Picture from http://cdn.physorg.com/newman/gfx/news/hires/nanoparticle.jpg

## Slide 43: Carrier (exiton) multiplication
Carrier multiplication is a phenomena where (probably) the carrier rapidly falls down to the ground level and the excess energy is used to excite up a second carrier or three
It happens all the time but have to compete with much more likely mechanics
Is especially interesting for photovoltaics
http://ej.iop.org/images/0957-4484/24/4/042001/Full/nano452232f3_online.jpg